Supplementary Information

Toward transparent rigid packaging from sugarcane bagasse: a consistency-testing framework for nanocellulose–chitosan sheets

Leon Sandler, Independent Researcher, Northbrook, Illinois, USA. sandler.leon@gmail.com

Contents: S1 optical screen (derivation, angular correction, calibration checks, full haze budget); S2 wet-stiffness screen; S3 forming geometry; S4 literature dataset, per-reference support and documented searches; S5 uncertainty propagation and sensitivity; S6 experimental matrix; S7 surface and coarse scattering; S8 prior schemes and the robustness panel; S9 thickness coupling; S10 wax-layer sensitivity. All numbers are produced by code/run_analysis.py (seed 20261002) and are reproduced by running that script.

# S1 Optical screen

## S1.1 Derivation of Eq. (2)

Take a medium whose permittivity fluctuates about its mean by δε(r) with correlation function ⟨δε(0)δε(r)⟩ = ⟨δε2⟩γ(r). In the first Born approximation the light scattered per unit volume into a unit solid angle at scattering angle θ, for unpolarised incident light of vacuum wavelength λ, is (Debye and Bueche 1949)

dΣdΩ = π2λ4 ⟨Δε2⟩ Γq 1 + cos2θ2	(S1)

where Γ(q) = ∫γ(r)eiq·rd3r and q = 2k sin(θ/2) with k = 2πn̄/λ. The factor (1 + cos2θ)/2 accounts for the polarisation of the scattered light. For an exponential correlation function γ(r) = exp(−r/a), the form that characterises random hole structures in a solid (Debye et al. 1957),

Γq = 8πa31 + q2a22	(S2)

For a solid cellulose phase of index nc and air voids of volume fraction φ, ⟨δε2⟩ = φ(1−φ)(nc2 − 1)2. Integrating Eq. (S1) over the sphere, with u = cos θ and q2 = 2k2(1−u), gives the scattering coefficient τ = 2π ∫ dΣ/dΩ du over u from −1 to 1. In the limit qa ≪ 1 this reduces to τ = (64π4/3)φ(1−φ)(Δε)2a3/λ4 (Eq. 2 with g = 1). The numerical factor follows from ∫(1+u2)/2 du = 4/3 over −1 to 1 together with the prefactor of Eq. (S1) and the Debye–Bueche value Γ(0) = 8πa3: 4π × π2 × 8π × (2/3) = 64π4/3 ≈ 2078. The exact angular integral relative to this limit is g(a). The code evaluates it by Gauss–Legendre quadrature (48 nodes) and splits the integral into the backward hemisphere, the forward hemisphere beyond 2.5° and the forward cone within 2.5°, which gives fh and the back-scattered fraction.

Check against an independent result. For dilute small spheres of volume V and index contrast close to one, the correlation integral reduces to Γ(0) = V, and Eq. (S1) integrated over angle must reproduce Rayleigh scattering, τ = Nσ with σ = (2π5/3)D6/λ4[(m2−1)/(m2+2)]2. The verification suite finds a ratio of 1.013 for D = 20 nm, φ = 10−3 and m = 1.01; the residual is the (m2+2) local-field factor, which the Born treatment omits.

## S1.2 The angular correction g(a)

Table S1 Angular correction to the cubic law for n̄ = 1.5 and λ = 550 nm: g is the exact turbidity relative to its small-feature limit; fh the share of scattered light that goes forward beyond 2.5°; fb the share scattered backward.

| a (nm) | g(a) | Cubic law overestimates τ by | fh | fb | kΔn a |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.999 | ×1.00 | 0.500 | 0.500 | 0.01 |
| 2 | 0.995 | ×1.00 | 0.501 | 0.499 | 0.01 |
| 5 | 0.972 | ×1.03 | 0.507 | 0.492 | 0.03 |
| 10 | 0.895 | ×1.12 | 0.530 | 0.469 | 0.06 |
| 15 | 0.793 | ×1.26 | 0.565 | 0.434 | 0.09 |
| 20 | 0.685 | ×1.46 | 0.606 | 0.393 | 0.13 |
| 30 | 0.498 | ×2.01 | 0.691 | 0.308 | 0.19 |
| 40 | 0.365 | ×2.74 | 0.765 | 0.233 | 0.25 |
| 60 | 0.214 | ×4.68 | 0.862 | 0.135 | 0.38 |
| 80 | 0.138 | ×7.23 | 0.912 | 0.083 | 0.50 |
| 120 | 0.071 | ×14.11 | 0.951 | 0.039 | 0.75 |

The last column, kΔn a with Δn = 0.55, is the phase shift across one correlation length. The Born approximation requires it to be small. It is 0.02 at 3 nm, 0.06 at 10 nm, 0.25 at 40 nm and 0.50 at 80 nm, so the approximation is comfortable at the wood-pulp fibril scale and marginal at the coarse end of the bagasse range (tens of nanometres and above), where results should be read as indicative.

## S1.3 Calibration checks

No fitting is done. The checks compare the screen with published values.

Haze of clear nanopaper at 40 µm (Hsieh et al. 2017: 4.9–11.7%; density 1.29–1.55 g cm−3; fibre width 3–15 nm). Wood-pulp-scale structure, 200,000 samples: haze quantiles (5, 25, 50, 75, 95%) = 0.0, 0.4, 1.5, 5.5, 23.4 %; 14% of samples inside the observed band, 73% below and 13% above. For the bagasse range the quantiles are 0.0, 3.8, 27.6, 89.1, 100.0 %, with 11% inside, 28% below and 61% above.

Radiative relation (Xu et al. 2016): from a reported direct transmittance the single-scattering slab gives a haze of 14.2% (direct 75.1%, reported haze 10.0%) and 52.6% (direct 31.1%, reported 62.0%). The relation is therefore good to about 10 percentage points, independent of any structural assumption.

Lowest reported haze. A haze of 1.4% at 91% transmittance has been reported for super-clear nanopaper from bagasse nanocrystals (Tao et al. 2017); the thickness is not given in the abstract, so it is not used as a quantitative check. It is, however, of the order of the median haze of the wood-pulp-scale screen at 40 µm (1.5%).

## S1.4 Complete haze budget

Table S2 Haze budget by thickness and target. τmax is the largest scattering coefficient compatible with the target at fh = 0.5; the budget is φ(1−φ)a3g (nm3, with nc = 1.55, fm = 1); amax is the largest correlation length at each void fraction using the full angular integral.

| t (µm) | Haze target | τmax (m−1) | Budget (nm3) | amax, φ = 1% | 2% | 5% | 10% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 40 | 5% | 2502 | 56.0 | 19.0 | 14.8 | 10.8 | 8.7 |
| 40 | 10% | 5017 | 112.3 | 24.9 | 19.1 | 13.8 | 11.0 |
| 100 | 5% | 1001 | 22.4 | 13.6 | 10.7 | 7.9 | 6.3 |
| 100 | 10% | 2007 | 44.9 | 17.5 | 13.7 | 10.0 | 8.0 |
| 200 | 5% | 500 | 11.2 | 10.6 | 8.4 | 6.2 | 5.0 |
| 200 | 10% | 1003 | 22.5 | 13.6 | 10.7 | 7.9 | 6.3 |

# S2 Wet-stiffness screen

Hydration interpolation. For the chitosan–moisture map the stiffness at hydration h (0 ambient, 1 water-saturated) is the linear interpolation between the dry rule of mixtures and the saturated value of Eq. (4):

Ehydw, h = Edryw − hEdryw − Ewetw	(S3)

with Edry(w) = (1−w)ψ(w)EC + wEH and ψ(w) = 1 + (ψ − 1)[1 − exp(−w/0.05)], so that w = 0 recovers plain CNF exactly. In an acidic liquid κH is replaced by κH,acid and ξ(w) is multiplied by the surviving fraction.

Table S3 Water-saturated stiffness (GPa), quantiles over 200,000 samples, and the share of samples meeting each assumed requirement.

| w (wt%) | Liquid | 5% | 25% | 50% | 75% | 95% | ≥ 0.5 | ≥ 1 | ≥ 2 | Helps |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | neutral | 0.17 | 0.38 | 0.85 | 1.90 | 4.15 | 66% | 45% | 23% | – |
| 0 | acid | 0.17 | 0.38 | 0.85 | 1.90 | 4.15 | 66% | 45% | 23% | – |
| 5 | neutral | 0.49 | 1.09 | 1.79 | 2.77 | 4.66 | 95% | 78% | 43% | 86% |
| 5 | acid | 0.24 | 0.53 | 0.99 | 1.83 | 3.70 | 77% | 50% | 22% | 54% |
| 10 | neutral | 0.59 | 1.32 | 2.13 | 3.22 | 5.21 | 97% | 85% | 54% | 86% |
| 10 | acid | 0.24 | 0.56 | 1.04 | 1.81 | 3.51 | 79% | 52% | 21% | 53% |
| 20 | neutral | 0.69 | 1.50 | 2.36 | 3.51 | 5.56 | 98% | 88% | 60% | 86% |
| 20 | acid | 0.24 | 0.57 | 1.03 | 1.74 | 3.24 | 79% | 51% | 19% | 49% |
| 30 | neutral | 0.74 | 1.52 | 2.34 | 3.42 | 5.33 | 99% | 90% | 60% | 84% |
| 30 | acid | 0.24 | 0.54 | 0.96 | 1.60 | 2.92 | 78% | 48% | 16% | 44% |

Attribution to cross-linking. At 20 wt% chitosan in a neutral liquid, with the cross-linking term removed on the same draws, the median change in wet stiffness is -0.10 GPa and chitosan helps in 35% of samples, against +1.08 GPa and 86% with it. Consistency with published values. The wet modulus of 4 GPa reported for water-soaked 80/20 films (Toivonen et al. 2015) is reached or exceeded by 18% of modelled samples (modelled 5, 25, 50, 75, 95% quantiles: 0.69, 1.50, 2.36, 3.51, 5.56 GPa). The ratio of 8.76/14.71 = 0.60 reported when chitosan was added to carrot nanofibre films (Szymańska-Chargot et al. 2019) lies inside the assumed range of ψ (0.5–1.1).

# S3 Forming geometry

Window condition. A blank of diameter D0 = LDR·db drawn into a container of surface area Acup must supply Acup − πD02/4 of area by stretching. With uniform equibiaxial thinning the mean tensile log-strain is ε = ½ ln[Acup/(πD02/4)] = εb − ln(LDR), with εb the strain budget of Eq. (8). The tensile limit ε ≤ εcrit gives LDR ≥ exp(εb − εcrit). The compressive circumferential log-strain at the flange edge, ln(D0/db) = ln(LDR), is limited by the wrinkling tolerance, so LDR ≤ exp(εwr). The two bounds are compatible exactly when εb − εcrit ≤ εwr, which is Eq. (10). For a straight-walled cup of depth h and diameter d the budget is ½ ln(1 + 4h/d), so the deepest cup a total tolerance ε can form has h/d = (e2ε − 1)/4 (Fig. 4b).

The peak is not below the mean. For any nonuniform distribution of the log-area strain over the sheet with a given mean, the maximum is at least the mean, so εb − ln(LDR) is a lower bound on the peak tensile strain. The verification suite tests this on random nonuniform splits. Friction at the punch radius and local thinning raise the peak further, so the window condition is necessary, not sufficient.

Table S4 Reference geometries (mm) and strain budgets.

| Geometry | db | dt | h | Acup (mm2) | Acup/footprint | εb | LDR, no stretching | Equivalent straight h/d |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tray (lid-like) | 100 | 120 | 12 | 13252 | 1.69 | 0.262 | 1.30 | 0.17 |
| Bowl | 100 | 150 | 50 | 29807 | 3.80 | 0.667 | 1.95 | 0.70 |
| Cup | 55 | 80 | 90 | 21644 | 9.11 | 1.105 | 3.02 | 2.03 |

Table S5 Total strain tolerance εcrit + εwr: extremes over all assumed ranges (corner enumeration; the function is monotone in every parameter, so the extremes lie at corners) and the share of samples with a forming window.

| Hydration | Minimum | Maximum | Tray | Bowl | Cup |
| --- | --- | --- | --- | --- | --- |
| Ambient | 0.056 | 0.660 | 65.9% | 0.0% | 0.0% |
| Half | 0.061 | 0.810 | 77.3% | 1.2% | 0.0% |
| Saturated | 0.066 | 0.960 | 85.5% | 6.9% | 0.0% |

Budgets are 0.262 (tray), 0.667 (bowl) and 1.105 (cup). The cup budget exceeds the largest tolerance reachable at any hydration (0.960 at saturation), so no sampling can open a window; the bowl budget lies between the ambient maximum (0.660) and the half-hydrated maximum (0.810).

# S4 Literature dataset, support and searches

How the evidence was handled. Each reference was resolved against its Crossref record by script (references/harvest.py) and compared with the intended author, year and title; mismatches were investigated before use. This found that all three of the transparency references in the first version of this manuscript were wrongly attributed (wrong first author, wrong pages or both); they are corrected here. Each statement was then checked against the cited source’s abstract where one could be retrieved (Crossref, PubMed, OpenAlex or Semantic Scholar). Table S7 states, for every reference, whether the statements attached to it rest on an abstract that was read or are limited to what the title says. Full texts were not available to the verification process.

Table S6 Numerical anchors taken from the literature and where each is used.

| Quantity | Value | Source | Used for |
| --- | --- | --- | --- |
| Total transmittance, clear nanopaper, 40 µm | 89.3–91.5% | Hsieh et al. 2017 | Context; Table 1 |
| Haze, clear nanopaper, 40 µm | 4.9–11.7% | Hsieh et al. 2017 | Calibration check (S1.3) |
| Density, clear nanopaper | 1.29–1.55 g cm−3 | Hsieh et al. 2017 | Range of ρf |
| Fibre width, clear nanopaper | 3–15 nm | Hsieh et al. 2017 | Range of a (wood-pulp scale) |
| TOCN width | 3–4 nm | Fukuzumi et al. 2009 | Lower end of a |
| Bagasse nanofibril diameter, microfluidised | 5–80 nm | Carneiro Pessan et al. 2023 | Range of a (bagasse) |
| Direct transmittance and haze, hybrid CNF/CNC | 75.1% and 10.0% (earlier: 31.1% and 62.0%) | Xu et al. 2016 | Radiative-relation check |
| Transmittance and haze, bagasse CNC nanopaper | 91% and 1.4% (thickness not given) | Tao et al. 2017 | H1 framing |
| Rice-straw CNF film transmittance | 13–42% | Jiang et al. 2016 | H1 framing |
| Neat CNF film modulus | 4.79 GPa; about 4 GPa | Qing et al. 2012; Jiang et al. 2016 | Range of EC |
| Carrot CNF film modulus, with and without chitosan | 14.71 to 8.76 GPa at 5 wt% | Szymańska-Chargot et al. 2019 | Range of ψ; EC upper bound |
| Neat chitosan film modulus; elongation | 2.3–3.4 GPa; above 13% | Fernández-Marín et al. 2024 | Range of EH |
| 80/20 CNF/chitosan, wet | 100 MPa, 28% strain, 4 GPa at 0.5% strain | Toivonen et al. 2015 | Consistency check; Δεw |
| 80/20 CNF/chitosan, 50% RH | 200 MPa, 8% strain | Toivonen et al. 2015 | Range of εf0 |
| Rice-straw CNF film strain at break | 16% | Jiang et al. 2016 | Range of εf0 |
| Porous TEMPO nanopaper | 56% porosity, 1.4 GPa, 17% strain to failure | Sehaqui et al. 2011 | Ductility-clarity tension |
| World sugarcane production, 2022 | 1,921 Mt | FAO 2024 | Context |
| Bagasse composition | 42% cellulose, 25% hemicellulose, 20% lignin | Kim and Day 2011 | Context |
| Refining energy to barrier plateau | 1,800–12,000 kWh t−1 | Kargupta et al. 2022 | Section 9 |
| Aqueous counter-collision defibrillation, rice straw | 15 kWh kg−1 | Jiang et al. 2016 | Section 9 |

Table S7 Support classification for every reference. ‘Abstract’: the statements attached to it were checked against an abstract that was read. ‘Title’: no abstract could be retrieved and the attached statements are limited to what the title states. ‘Dataset’: a primary data record.

| Reference | Support |
| --- | --- |
| Arvidsson R, Nguyen D, Svanström M (2015) Life cycle assessment of cellulose nanofibrils production by mechanical treatment and two different pretreatment processes. Environ Sci Technol 49:6881–6890. | Abstract |
| ASTM International (2021) ASTM D1003-21: standard test method for haze and luminous transmittance of transparent plastics. ASTM International, West Conshohocken, PA. | Abstract |
| Aulin C, Gällstedt M, Lindström T (2010) Oxygen and oil barrier properties of microfibrillated cellulose films and coatings. Cellulose 17:559–574. | Title |
| Azeredo HM, Mattoso LHC, Avena‐Bustillos RJ et al (2010) Nanocellulose reinforced chitosan composite films as affected by nanofiller loading and plasticizer content. J Food Sci 75(1). | Abstract |
| Azeredo HM, Rosa MF, Mattoso LHC (2017) Nanocellulose in bio-based food packaging applications. Ind Crops Prod 97:664–671. | Title |
| Benítez AJ, Walther A (2017) Cellulose nanofibril nanopapers and bioinspired nanocomposites: a review to understand the mechanical property space. J Mater Chem A 5:16003–16024. | Abstract |
| Bhattacharya D, Germinario LT, Winter WT (2008) Isolation, preparation and characterization of cellulose microfibers obtained from bagasse. Carbohydr Polym 73:371–377. | Title |
| Carneiro Pessan C, Silva Bernardes J, Bettini SH et al (2023) Oxidized cellulose nanofibers from sugarcane bagasse obtained by microfluidization: Morphology and rheological behavior. Carbohydr Polym 304:120505. | Abstract |
| Debye P, Bueche AM (1949) Scattering by an inhomogeneous solid. J Appl Phys 20:518–525. | Abstract |
| Debye P, Anderson HR, Brumberger H (1957) Scattering by an inhomogeneous solid. II. The correlation function and its application. J Appl Phys 28:679–683. | Abstract |
| Fang Z, Zhu H, Bao W et al (2014) Highly transparent paper with tunable haze for green electronics. Energy Environ Sci 7:3313–3319. | Abstract |
| FAO (2024) FAOSTAT: crops and livestock products, sugar cane (item 156), production quantity (element 5510), world total. Food and Agriculture Organization of the United Nations, Rome. | Dataset |
| Fernández-Marín R, Morales A, Erdocia X et al (2024) Chitosan–chitin nanocrystal films from lobster and spider crab: properties and environmental sustainability. ACS Sustain Chem Eng 12:10363–10375. | Abstract |
| Fukuzumi H, Saito T, Iwata T et al (2009) Transparent and high gas barrier films of cellulose nanofibers prepared by TEMPO-mediated oxidation. Biomacromolecules 10:162–165. | Abstract |
| Fukuzumi H, Saito T, Isogai A (2013) Influence of TEMPO-oxidized cellulose nanofibril length on film properties. Carbohydr Polym 93:172–177. | Abstract |
| Ghormade V, Pathan E, Deshpande M (2017) Can fungi compete with marine sources for chitosan production? Int J Biol Macromol 104:1415–1421. | Abstract |
| Guzman-Puyol S, Benítez JJ, Heredia-Guerrero JA (2022) Transparency of polymeric food packaging materials. Food Res Int 161:111792. | Abstract |
| Hauptmann M, Majschak J (2011) New quality level of packaging components from paperboard through technology improvement in 3D forming. Packag Technol Sci 24:419–432. | Abstract |
| Henriksson M, Berglund LA, Isaksson P et al (2008) Cellulose nanopaper structures of high toughness. Biomacromolecules 9:1579–1585. | Abstract |
| Hiranobe CT, Gomes AS, Paiva FFG et al (2024) Sugarcane bagasse: challenges and opportunities for waste recycling. Clean Technol 6:662–699. | Abstract |
| Hsieh M-C, Koga H, Suganuma K et al (2017) Hazy transparent cellulose nanopaper. Sci Rep 7:41590. | Abstract |
| Hubbe MA, Ferrer A, Tyagi P et al (2017) Nanocellulose in thin films, coatings, and plies for packaging applications: a review. BioResources 12:2143–2233. | Abstract |
| Isogai A, Saito T, Fukuzumi H (2011) TEMPO-oxidized cellulose nanofibers. Nanoscale 3:71–85. | Title |
| Jiang F, Kondo T, Hsieh Y-L (2016) Rice straw cellulose nanofibrils via aqueous counter collision and differential centrifugation and their self-assembled structures. ACS Sustain Chem Eng 4:1697–1706. | Abstract |
| Jäger K, Zeman M (2009) A scattering model for surface-textured thin films. Appl Phys Lett 95:171108. | Abstract |
| Kabeyi MJB, Olanrewaju OA (2023) Bagasse electricity potential of conventional sugarcane factories. J Energy 2023:1–25. | Abstract |
| Kargupta W, Seifert R, Martinez M et al (2022) Preparation and benchmarking of novel cellulose nanopaper. Cellulose 29:4393–4411. | Abstract |
| Kim M, Day DF (2011) Composition of sugar cane, energy cane, and sweet sorghum suitable for ethanol production at Louisiana sugar mills. J Ind Microbiol Biotechnol 38:803–807. | Abstract |
| Klemm D, Kramer F, Moritz S et al (2011) Nanocelluloses: a new family of nature‐based materials. Angew Chem Int Ed 50:5438–5466. | Title |
| Lavoine N, Desloges I, Dufresne A et al (2012) Microfibrillated cellulose – Its barrier properties and applications in cellulosic materials: a review. Carbohydr Polym 90:735–764. | Abstract |
| Li W, Wang S, Wang W et al (2019) Facile preparation of reactive hydrophobic cellulose nanofibril film for reducing water vapor permeability (WVP) in packaging applications. Cellulose 26:3271–3284. | Title |
| Lyu D, Tang Y, Qian L et al (2019) Large strain cavitation induced stress whitening in propylene-butene-1 copolymer during stretching. Polymer 167:146–153. | Abstract |
| Mandal A, Chakrabarty D (2011) Isolation of nanocellulose from waste sugarcane bagasse (SCB) and its characterization. Carbohydr Polym 86:1291–1299. | Title |
| Melro E, Antunes FE, da Silva GJ et al (2021) Chitosan films in food applications. Tuning film properties by changing acidic dissolution conditions. Polymers 13:1. | Abstract |
| Moon RJ, Martini A, Nairn J et al (2011) Cellulose nanomaterials review: structure, properties and nanocomposites. Chem Soc Rev 40:3941. | Title |
| Mäkelä T, Kainlauri M, Willberg-Keyriläinen P et al (2016) Fabrication of micropillars on nanocellulose films using a roll-to-roll nanoimprinting method. Microelectron Eng 163:1–6. | Abstract |
| Ndikumana S, Tanane O, Aichi Y et al (2025) Innovative applications of sugarcane bagasse in the global sugarcane industry. Processes 13:3796. | Abstract |
| Nechyporchuk O, Belgacem MN, Bras J (2016) Production of cellulose nanofibrils: a review of recent advances. Ind Crops Prod 93:2–25. | Title |
| Niskanen I, Zhang K, Karzarjeddi M et al (2022) Optical properties of cellulose nanofibre films at high temperatures. J Polym Res 29:187. | Abstract |
| Nogi M, Iwamoto S, Nakagaito AN et al (2009) Optically transparent nanofiber paper. Adv Mater 21:1595–1598. | Abstract |
| Nogi M, Kim C, Sugahara T et al (2013) High thermal stability of optical transparency in cellulose nanofiber paper. Appl Phys Lett 102:181911. | Abstract |
| Otenda BV, Kareru PG, Madivoli ES et al (2022) Cellulose nanofibrils from sugarcane bagasse as a reinforcing element in polyvinyl alcohol composite films for food packaging. J Nat Fibers 19:3585–3597. | Abstract |
| Pillai C, Paul W, Sharma CP (2009) Chitin and chitosan polymers: Chemistry, solubility and fiber formation. Prog Polym Sci 34:641–678. | Title |
| Qing Y, Sabo R, Wu Y et al (2012) High-performance cellulose nanofibril composite films. BioResources 7:3064–3075. | Abstract |
| Rinaudo M (2006) Chitin and chitosan: properties and applications. Prog Polym Sci 31:603–632. | Title |
| Rol F, Billot M, Bolloli M et al (2020) Production of 100% cellulose nanofibril objects using the molded cellulose process: a feasibility study. Ind Eng Chem Res 59:7670–7679. | Abstract |
| Saito T, Kimura S, Nishiyama Y et al (2007) Cellulose nanofibers prepared by TEMPO-mediated oxidation of native cellulose. Biomacromolecules 8:2485–2491. | Title |
| Scopel E, Pinto LO, Rezende CA (2025) Residual lignin affects production and properties of TEMPO-oxidized cellulose nanofibrils from partially delignified sugarcane bagasse. Cellulose 32:9315–9331. | Title |
| Sehaqui H, Zhou Q, Ikkala O et al (2011) Strong and tough cellulose nanopaper with high specific surface area and porosity. Biomacromolecules 12:3638–3644. | Abstract |
| Sellman FA, Rostami J, Östmans R et al (2024) Influence of fibril aspect ratio, chemical functionality, and volume fraction on the mechanical properties of cellulose nanofibril materials. Cellulose 31:8007–8025. | Abstract |
| Semple KE, Zhou C, Rojas OJ et al (2022) Moulded pulp fibers for disposable food packaging: a state-of-the-art review. Food Packag Shelf Life 33:100908. | Abstract |
| Shimizu M, Saito T, Isogai A (2016) Water-resistant and high oxygen-barrier nanocellulose films with interfibrillar cross-linkages formed through multivalent metal ions. J Membr Sci 500:1–7. | Title |
| Sirviö JA, Kantola AM, Komulainen S et al (2021) Aqueous modification of chitosan with itaconic acid to produce strong oxygen barrier film. Biomacromolecules 22:2119–2128. | Abstract |
| Spence KL, Venditti RA, Rojas OJ et al (2011) A comparative study of energy consumption and physical properties of microfibrillated cellulose produced by different processing methods. Cellulose 18:1097–1111. | Title |
| Szymańska-Chargot M, Chylińska M, Pertile G et al (2019) Influence of chitosan addition on the mechanical and antibacterial properties of carrot cellulose nanofibre film. Cellulose 26:9613–9629. | Abstract |
| Tao J, Fang Z, Zhang Q et al (2017) Super‐clear nanopaper from agro‐industrial waste for green electronics. Adv Electron Mater 3:1600539. | Abstract |
| Toivonen MS, Kurki-Suonio S, Schacher FH et al (2015) Water-resistant, transparent hybrid nanopaper by physical cross-linking with chitosan. Biomacromolecules 16:1062–1071. | Abstract |
| Vishtal A, Retulainen E (2012) Deep-drawing of paper and paperboard: the role of material properties. BioResources 7:4424–4450. | Abstract |
| Wang Y, He B, Zhao L (2017) Fabrication of hydrophobic coating on filter paper from self-emulsifying carnauba wax-alcohol emulsions with nano-TiO2 particles for water/diesel separation. BioResources 12:7774–7783. | Abstract |
| Xu X, Zhou J, Jiang L et al (2016) Highly transparent, low-haze, hybrid cellulose nanopaper as electrodes for flexible electronics. Nanoscale 8:12294–12306. | Abstract |
| Yang W, Jiao L, Liu W et al (2019) Manufacture of highly transparent and hazy cellulose nanofibril films via coating TEMPO-oxidized wood fibers. Nanomaterials 9:107. | Abstract |
| Zhu H, Fang Z, Preston C et al (2014) Transparent paper: fabrications, properties, and device applications. Energy Environ Sci 7:269–287. | Title |

Documented searches behind the statements of absence. Searches were run on 2 October 2026 against the OpenAlex works index (journal articles, relevance-ranked), the first 12 titles of each were read, and a hit was counted only if it concerned the thing searched for. The full record is in references/search_log.md. Summary:

Forming of dense nanocellulose sheets (queries F1–F4: thermoforming, deep drawing, thermoformable three-dimensional shaping, hot-pressing moulds). Relevant results: Rol et al. 2020 (wet moulding of CNF mats: objects obtained, none transparent and dimensionally stable because of drying shrinkage), Mäkelä et al. 2016 (thermal roll-to-roll imprinting of brittle, non-thermoplastic CNF films, micrometre-scale patterns only) and Semple et al. 2022 (moulded pulp review, opaque pulp products). No report was found of a transparent dense nanocellulose sheet formed into a three-dimensional shape.

Transparent sheets from bagasse (B1–B3). Relevant results: Tao et al. 2017 (super-clear nanopaper from bagasse nanocrystals, 91% transmittance, 1.4% haze). No optical data for a transparent sheet made from bagasse nanofibrils were found; the bagasse nanofibril studies found (Carneiro Pessan et al. 2023; Otenda et al. 2022) characterise the nanofibrils and composite films.

Wax-coated and chitosan-containing transparent cellulose films (W1, C1). The CNF/chitosan wet-strength result of Toivonen et al. 2015 was the only directly relevant hit. A claim carried over from the first version, of transparent carbamylated CNF films with a water contact angle near 109°, could not be traced to any source and has been removed.

These are searches of one index by title and abstract, not systematic reviews; absence from them is evidence, not proof, of absence from the literature.

Final audit. Before submission every cited DOI was re-resolved against Crossref (references/audit_refs.py; references/audit_log.md): 59 records matched the cached title, first author, journal and volume, none carried a retraction or withdrawal notice, and 19 numerical or qualitative anchors used in the text and in Table 3 were located in the cited abstracts (for example 4.9–11.7% haze and 1.29–1.55 g cm−3 in Hsieh et al. 2017, 8.76 and 14.71 GPa in Szymańska-Chargot et al. 2019, 28% and 4 GPa in Toivonen et al. 2015). Numbers that sit only in a full text were not checked.

# S5 Uncertainty propagation and sensitivity

Sampling. N = 200,000 per test; seed 20261002 (NumPy default_rng, offsets +1, +10, +20, +30, +40, +50 for the calibration, optical, mechanical, forming, joint and sensitivity draws, and +60 to +100 for the extensions, so the streams are independent). Parameters are drawn independently from the registry (Table 3 of the main text), uniformly or log-uniformly; the void fraction is derived from the sampled film and wall densities and clipped to 0–0.5. A sample passes a test when its haze, wet stiffness or forming window meets the stated requirement; the joint share is the share of samples passing all three.

Table S8 Spearman rank correlation of each input with the output.

| Output | Input | ρ |
| --- | --- | --- |
| Haze, bagasse range, 100 µm | correlation length a | +0.803 |
| Haze, bagasse range, 100 µm | film density | -0.368 |
| Haze, bagasse range, 100 µm | morphology factor | +0.256 |
| Haze, bagasse range, 100 µm | wall density | +0.168 |
| Haze, bagasse range, 100 µm | refractive index | +0.057 |
| Haze, wood-pulp scale, 100 µm | correlation length a | +0.735 |
| Haze, wood-pulp scale, 100 µm | film density | -0.435 |
| Haze, wood-pulp scale, 100 µm | morphology factor | +0.338 |
| Haze, wood-pulp scale, 100 µm | wall density | +0.186 |
| Haze, wood-pulp scale, 100 µm | refractive index | +0.076 |
| Ewet, 20 wt% chitosan, neutral | xi_max | +0.640 |
| Ewet, 20 wt% chitosan, neutral | E_cnf | +0.515 |
| Ewet, 20 wt% chitosan, neutral | kappa_cnf | +0.328 |
| Ewet, 20 wt% chitosan, neutral | psi | +0.316 |
| Ewet, 20 wt% chitosan, neutral | w_star | -0.128 |
| Ewet, 20 wt% chitosan, neutral | kappa_chi | +0.075 |
| Ewet, 20 wt% chitosan, neutral | E_chi | +0.027 |
| Ewet, 20 wt% chitosan, acid | kappa_cnf | +0.696 |
| Ewet, 20 wt% chitosan, acid | E_cnf | +0.414 |
| Ewet, 20 wt% chitosan, acid | xi_acid | +0.289 |
| Ewet, 20 wt% chitosan, acid | xi_max | +0.288 |
| Ewet, 20 wt% chitosan, acid | psi | +0.257 |
| Ewet, 20 wt% chitosan, acid | w_star | -0.062 |
| Ewet, 20 wt% chitosan, acid | kappa_chi_acid | +0.028 |
| Ewet, 20 wt% chitosan, acid | E_chi | +0.012 |
| Ewet, 20 wt% chitosan, acid | kappa_chi | +0.004 |
| Forming margin, bowl, saturated | eps_wrinkle | +0.855 |
| Forming margin, bowl, saturated | r_void | +0.388 |
| Forming margin, bowl, saturated | d_eps_wet | +0.266 |
| Forming margin, bowl, saturated | eps_f_dry | +0.137 |

Table S9 Joint share of sampled designs passing all three tests (reference design: 100 µm, 20 wt% chitosan, haze ≤ 10%, Ewet ≥ 1 GPa, forming at saturation).

| Range | Liquid | Geometry | Optical | Mechanical | Forming | All three |
| --- | --- | --- | --- | --- | --- | --- |
| wood-pulp scale | neutral | tray | 69% | 88% | 86% | 52.5% |
| wood-pulp scale | neutral | bowl | 69% | 88% | 7% | 4.3% |
| wood-pulp scale | neutral | cup | 69% | 88% | 0% | 0.0% |
| wood-pulp scale | acid | tray | 69% | 51% | 86% | 30.4% |
| wood-pulp scale | acid | bowl | 69% | 51% | 7% | 2.5% |
| wood-pulp scale | acid | cup | 69% | 51% | 0% | 0.0% |
| bagasse range | neutral | tray | 26% | 88% | 86% | 19.3% |
| bagasse range | neutral | bowl | 26% | 88% | 7% | 1.5% |
| bagasse range | neutral | cup | 26% | 88% | 0% | 0.0% |
| bagasse range | acid | tray | 26% | 51% | 86% | 11.2% |
| bagasse range | acid | bowl | 26% | 51% | 7% | 0.9% |
| bagasse range | acid | cup | 26% | 51% | 0% | 0.0% |

# S6 Experimental matrix

The matrix lists what each phase would measure, how, and what outcome would count against the framework. Thresholds marked ‘derived’ follow from the screens; those marked ‘proposed’ are design choices, not results.

| Phase | Measurement | Method / standard | Threshold | Origin |
| --- | --- | --- | --- | --- |
| I Material | Fibril width and length; crystallinity; density | AFM or TEM; XRD; helium pycnometry and thickness | Report; compare bagasse with wood pulp | – |
| I Material | Void fraction and correlation length | Small-angle X-ray scattering, Debye–Bueche plot | φ(1−φ)a3 ≤ 22 nm3 (100 µm, 5% haze); a ≤ 10 nm at 5% voids (100 µm, 10% haze) | Derived |
| I Material | Haze and transmittance versus thickness | ASTM D1003 at 40, 100, 200 µm; report thickness | Haze ∝ t (bulk) or constant (surface) | Derived |
| I Material | Surface roughness of both faces; coarse scatterers in the bulk | AFM or optical profilometry; microscopy, wide-angle scattering | Two-face haze from roughness ≤ 1%; coarse volume fraction below the haze budget (S7) | Derived |
| I Material | Effect of delignification and bleaching | Haze, colour, lignin content | Haze within budget at target thickness | Proposed |
| II Composite | Wet and dry tensile properties at 0, 5, 10, 20, 30 wt% chitosan | Tensile test, saturated and 50% RH | Ewet ≥ 1 GPa; gain over plain CNF > 0 | Proposed / derived |
| II Composite | Acid exposure | Wet modulus after soaking in acidic liquids | Gain near zero is the prediction | Derived |
| II Composite | Optical effect of chitosan | Haze, SAXS | No rise in φ(1−φ)a3 | Derived |
| III Barrier | Wax layer: thickness, haze, contact angle, liquid hold, abrasion | Profilometry; ASTM D1003; goniometry; 24 h hold; abrasion test | Added haze ≤ 1 point (S10); 24 h hold | Proposed / derived |
| IV Forming | Biaxial strain to failure, ambient and wet; in situ haze versus strain | Bulge test with optical haze | Total tolerance ≥ 0.26 (tray), 0.67 (bowl) | Derived |
| IV Forming | Wrinkling tolerance | Draw test with blank holder; LDR at wrinkle onset | LDRmax ≥ 1.30 (tray) | Derived |
| IV Forming | Shrinkage on drying of any wet-formed part | Dimensional change; haze after drying | Report (not modelled) | Rol et al. 2020 |
| V Package | Filled-container drop; lid attachment; thermal cycling; extended containment | Drop from 1 m; seal test; cycling | No failure | Proposed |

# S7 Surface and coarse scattering (main text Sections 5.6 and 6.5)

These bounded additions test how far the optical conclusions depend on what the core screen omits. All ranges are assumptions (Table S10); none enters the 19-parameter registry or the numbers of main-text Sections 6.1–6.4, which are unchanged by them (results.json sections A–G are identical in the v1.0.0 and later runs).

Table S10 Registry of the parameters of the bounded extensions. Every range is an assumption.

| Parameter | Range | Unit | Dist. | Meaning |
| --- | --- | --- | --- | --- |
| sigma_surf | 1 – 30 | nm | lu | RMS height of each film surface (two surfaces); no measurement is cited |
| f_surf | 0.3 – 1 | - | u | Fraction of surface-scattered light deviating by more than 2.5 deg |
| phi_coarse | 1e-05 – 0.0003 | - | lu | Volume fraction of a coarse void or fragment population (residual fibres, aggregates); set from the inverse calculation of run_analysis.py section H so that it is detectable only by its haze |
| a_coarse | 50 – 300 | nm | lu | Correlation length of the coarse population |
| t_wax | 0.2 – 1 | um | u | Thickness of the sub-micron wax layer |
| n_wax | 1.4 – 1.5 | - | u | Refractive index of the wax |
| sigma_wax | 3 – 50 | nm | lu | RMS height of the wax surface |
| dn_wax | 0.02 – 0.1 | - | u | Index contrast between wax crystallites and amorphous wax |
| phi_wax | 0.05 – 0.3 | - | u | Volume fraction of wax crystallites |
| a_wax | 50 – 300 | nm | lu | Correlation length of the wax crystallite structure |
| eps_wax | 0.01 – 0.1 | - | u | Tensile strain at which the wax layer cracks and stops holding liquid |

## S7.1 Rough-surface term

A thin rough interface with zero-mean height h(x, y) of RMS value σ imposes on a transmitted plane wave the phase (2π/λ)(nf − nout) h. For Gaussian heights and small slopes the coherent amplitude is exp(−Φ²/2), with

Φ = 2πnf − noutσλ	(S3)

so the specular transmitted fraction is exp(−Φ²) and the fraction scattered is 1 − exp(−Φ²). The fraction beyond the 2.5° cone is fs times that, where fs (0.3–1, assumed) stands in for the lateral correlation length of the roughness, which is not represented: long correlation lengths concentrate the scattered light at small angles. The small-roughness limit is fsΦ². The relation holds for σ much smaller than λ/[2π(n − 1)], about 175 nm. For two identical faces the roughness that alone gives a haze H follows from 1 − (1 − s)² = H:

σ = λ2πnf − 1−ln1 − 1 − 1 − Hfs	(S4)

Evaluated with nf = 1.5: σ = 27.7 nm for H = 4.9%, 35.7 nm for 8% and 43.7 nm for 11.7% (fs = 1); 67.0 nm for 8% if only 30% of the scattered light leaves the cone. The haze of two faces is 0.16%, 0.65%, 2.58% and 5.70% at σ = 5, 10, 20 and 30 nm.

## S7.2 Combining faces, network and coarse population

Light is followed through the entrance face, the nanofibril network, the coarse population and the exit face, with the state (D, F) of direct and diffuse fractions starting at (1, 0). A face of scattered fraction s moves s·D from D to F. A bulk layer of optical depth x and forward-haze fraction fh moves fhD(1 − e−x) from D to F and multiplies D by e−x. The haze is F/(D + F). With zero face terms and no coarse population this is exactly Eq. (3) of the main text (checked in the verification suite). The bookkeeping scatters each ray at most once per element and does not attenuate light that is already diffuse, so it is an estimate, optimistic at large optical depth, like Eq. (3).

Table S11 Haze of a wood-pulp-scale sheet (5th, 25th, 50th, 75th, 95th percentile, %) and the share of samples inside, below and above the observed 4.9–11.7% band, by thickness and scattering included.

| Thickness | Scattering | Percentiles 5/25/50/75/95 | Inside | Below | Above |
| --- | --- | --- | --- | --- | --- |
| 40 µm | bulk only | 0.0 / 0.4 / 1.5 / 5.5 / 23.5 | 14% | 73% | 13% |
| 40 µm | + surfaces | 0.1 / 0.8 / 2.3 / 6.2 / 24.0 | 17% | 69% | 14% |
| 40 µm | + coarse | 0.5 / 1.6 / 3.8 / 8.6 / 25.3 | 25% | 58% | 17% |
| 40 µm | + both | 0.7 / 2.2 / 4.6 / 9.2 / 25.8 | 29% | 53% | 18% |
| 100 µm | bulk only | 0.0 / 1.0 / 3.6 / 13.6 / 52.8 | 17% | 56% | 28% |
| 100 µm | + surfaces | 0.3 / 1.5 / 4.5 / 14.1 / 53.1 | 19% | 52% | 29% |
| 100 µm | + coarse | 1.3 / 4.1 / 9.4 / 20.5 / 55.6 | 27% | 30% | 43% |
| 100 µm | + both | 1.6 / 4.7 / 10.0 / 21.0 / 55.9 | 29% | 26% | 44% |
| 200 µm | bulk only | 0.0 / 1.9 / 7.3 / 26.5 / 81.9 | 17% | 42% | 41% |
| 200 µm | + surfaces | 0.4 / 2.6 / 8.0 / 27.0 / 82.1 | 19% | 39% | 42% |
| 200 µm | + coarse | 2.6 / 8.0 / 18.1 / 37.9 / 84.0 | 22% | 14% | 64% |
| 200 µm | + both | 3.0 / 8.6 / 18.7 / 38.3 / 84.1 | 23% | 12% | 66% |

Table S12 Inverse calculation: the coarse volume fraction that alone gives 8% haze at 40 µm, and the haze it implies thicker. Largest correlation length a (nm) for 100 µm, 10% haze and 5% voids once a baseline is present.

| Coarse size (nm) | Volume fraction | Haze at 100 µm | Haze at 200 µm |
| --- | --- | --- | --- |
| 50 | 0.1697% | 19.0% | 34.9% |
| 100 | 0.0542% | 18.9% | 34.3% |
| 200 | 0.0226% | 18.9% | 34.2% |
| 300 | 0.0147% | 18.9% | 34.3% |

Largest correlation length at 100 µm, 10% haze and 5% voids: 10.0 nm with no baseline; 10.0, 9.8 and 9.0 nm with face roughness of 5, 10 and 20 nm RMS; 9.9 and 9.4 nm with a 100 nm coarse population of 0.001% and 0.005%.

# S8 Prior schemes and the full robustness panel (main text Section 6.7)

Each scheme draws all 19 parameters independently (N = 200,000, streams seed + 100 + k). Literature-informed ranges are left unchanged by the last four schemes; the schemes act on the 11 assumed ranges.

| Scheme | Definition |
| --- | --- |
| base | Uniform, or log-uniform where the range spans an order of magnitude (the distributions of the main text) |
| uniform | Uniform in linear space for every parameter |
| centred | Triangular, mode at the middle of the range (geometric middle for log-uniform) |
| widened | Assumed ranges widened by 50% of their width on each side, clipped to physical limits (e.g. wrinkle tolerance 0–0.725, nc 1.44–1.68) |
| narrowed | Assumed ranges narrowed to their central 50% |
| optimistic | Assumed parameters triangular with the mode at the end of the range that helps the test |
| pessimistic | Assumed parameters triangular with the mode at the end of the range that hurts the test |

Table S13 Outputs of Sections 6.1–6.4 under the seven prior schemes (fractions of samples unless stated).

| Output | base | uniform | centred | widened | narrowed | optimistic | pessimistic |
| --- | --- | --- | --- | --- | --- | --- | --- |
| P_haze10_ref_t100 | 0.693 | 0.462 | 0.499 | 0.684 | 0.695 | 0.802 | 0.572 |
| P_haze10_bag_t100 | 0.255 | 0.094 | 0.021 | 0.300 | 0.243 | 0.349 | 0.161 |
| P_haze10_bag_t200 | 0.179 | 0.073 | 0.012 | 0.238 | 0.159 | 0.270 | 0.092 |
| median_haze40_ref_pct | 1.474 | 4.827 | 4.034 | 1.336 | 1.492 | 0.752 | 2.818 |
| calibration_in_band_ref40 | 0.141 | 0.195 | 0.265 | 0.116 | 0.152 | 0.112 | 0.171 |
| P_helps_neutral | 0.859 | 0.704 | 0.864 | 0.821 | 0.990 | 0.891 | 0.896 |
| P_helps_acid | 0.488 | 0.260 | 0.311 | 0.633 | 0.621 | 0.548 | 0.409 |
| median_E_neutral_w20_GPa | 2.355 | 2.807 | 2.737 | 2.759 | 2.297 | 3.336 | 1.396 |
| median_E_acid_w20_GPa | 1.023 | 1.656 | 1.461 | 1.308 | 0.976 | 1.770 | 0.487 |
| median_gain_neutral_GPa | 1.075 | 0.565 | 0.924 | 1.296 | 1.319 | 1.458 | 0.716 |
| median_gain_acid_GPa | -0.010 | -0.357 | -0.210 | 0.169 | 0.086 | 0.078 | -0.035 |
| P_E_ge_1_neutral | 0.886 | 0.951 | 0.987 | 0.896 | 0.968 | 0.988 | 0.676 |
| P_E_ge_1_acid | 0.511 | 0.758 | 0.764 | 0.601 | 0.482 | 0.816 | 0.185 |
| P_window_tray | 0.854 | 0.855 | 0.948 | 0.828 | 0.988 | 0.981 | 0.651 |
| P_window_bowl | 0.070 | 0.070 | 0.016 | 0.275 | 0.003 | 0.191 | 0.006 |
| P_window_cup | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| best_case_total_tolerance_saturated | 0.960 | 0.960 | 0.960 | 1.185 | 0.756 | 0.960 | 0.960 |
| cup_possible_in_range | no | no | no | yes | no | no | no |
| P_all_ref_tray | 0.525 | 0.376 | 0.466 | 0.508 | 0.664 | 0.777 | 0.251 |
| P_all_ref_bowl | 0.043 | 0.031 | 0.008 | 0.169 | 0.002 | 0.152 | 0.002 |
| P_all_ref_cup | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| P_all_bag_tray | 0.193 | 0.077 | 0.019 | 0.223 | 0.232 | 0.338 | 0.070 |
| P_all_bag_bowl | 0.016 | 0.006 | 0.000 | 0.074 | 0.001 | 0.066 | 0.001 |
| P_all_bag_cup | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

Statements that hold in all seven schemes: tray window > bowl window ≥ cup window (True); wood-pulp-scale optical pass share > bagasse-range (True); chitosan helps in more samples at neutral pH than in acid (True); median gain in acid < median gain at neutral pH (True). The cup has a non-zero window only in: widened.

What the cup needs. The strain budget of the cup is 1.105 and of the bowl 0.667. With every tensile tolerance at its best case (εcrit = 0.46, saturated), the flange must tolerate a wrinkling strain of 0.645 (limiting draw ratio 1.91) for the cup and 0.207 for the bowl; at the median tensile tolerance (0.15) the cup needs 0.956 (draw ratio 2.60). The assumed upper bound of the wrinkling tolerance is 0.50 (draw ratio 1.65).

# S9 Thickness coupling of the optical and stiffness screens (main text Section 6.6)

For a thin plate of modulus E, thickness t and Poisson ratio ν the flexural rigidity is E t³/[12(1 − ν²)]. Holding ν fixed, equal rigidity gives Eq. (12) of the main text,

tmin = trefErefE13	(S5)

which is physics only through its t⁻³ scaling. The anchor (Eref = 1 GPa at tref = 100 µm) is the reference requirement of the main text, an assumption. A different anchor moves tmin by the cube root of the ratio: the table gives the effect on the median minimum thickness and on the allowed correlation length (5% voids, 10% haze).

Table S14 Thickness coupling at 20 wt% chitosan: minimum thickness from the median wet modulus for three anchors, and the shares of samples meeting the 10% haze target at each sample’s own minimum thickness.

| Liquid | Median E (GPa) | Anchor Eref (GPa) | tmin median (µm) | tmin 5–95% (µm), anchor 1 GPa | amax at tmin (nm) | Haze pass: wood-pulp / bagasse |
| --- | --- | --- | --- | --- | --- | --- |
| neutral | 2.35 | 0.5 | 60 | – | 12.0 | – |
| neutral | 2.35 | 1.0 | 75 | 56–113 | 11.1 | 74% / 29% |
| neutral | 2.35 | 2.0 | 95 | – | 10.2 | – |
| acid | 1.03 | 0.5 | 79 | – | 10.9 | – |
| acid | 1.03 | 1.0 | 99 | 68–160 | 10.0 | 69% / 26% |
| acid | 1.03 | 2.0 | 125 | – | 9.3 | – |

# S10 Wax layer: bounded optical and forming sensitivity (main text Section 6.8)

The wax layer enters the optical bookkeeping of S7.2 in two ways: the wax–air face is a rough interface with the index of the wax and its own RMS height, and crystallites in the layer are a coarse scattering term with the contrast of crystalline against amorphous wax, Δεw = (nw + Δn)² − nw², in Eq. (2) with φw and aw and with optical depth τwtw. Haze added is the difference between the coated and the uncoated wall on the same film samples (wood-pulp scale, bulk only; one face coated). For forming, a coating applied before drawing cracks at the tensile strain εwax, so the tolerated tensile strain becomes min(εcrit, εwax). All ranges are in Table S10. Liquid containment is not modelled, and so no result here bears on whether the layer holds liquid.

Table S15 Wax-layer sensitivity (assumed ranges).

| Quantity | 100 µm wall | 200 µm wall |
| --- | --- | --- |
| Added haze, 5/25/50/75/95th percentile (points) | 0.13 / 0.45 / 1.04 / 2.18 / 4.76 | 0.08 / 0.37 / 0.91 / 1.99 / 4.51 |
| Share adding more than 1 point | 51% | 47% |
| Share adding more than 2 points | 28% | 25% |
| Share adding more than 5 points | 4% | 4% |
| Median added, wax face only (points) | 0.21 | 0.17 |
| Median added, crystallites only (points) | 0.47 | 0.41 |

| Geometry | Forming window, uncoated | Coated before forming |
| --- | --- | --- |
| tray | 85.5% | 64.9% |
| bowl | 6.9% | 0.0% |
| cup | 0.0% | 0.0% |

Spearman rank correlation of the added haze (100 µm) with the inputs: crystallite size a_wax +0.38; crystallite fraction phi_wax +0.20; index contrast dn_wax +0.45; layer thickness t_wax +0.22; wax roughness sigma_wax +0.56.

# Reproducing every number

From the repository root: python code/verify_model.py (58 checks); python code/run_analysis.py (writes code/results.json); python code/make_figures.py (writes the figures) and python code/export_figure_data.py (the numerical tables behind Figures 2–7); python manuscript/build_manuscript.py and python manuscript/build_si.py (rebuild the documents from results.json). References: python references/refs.py (formats the list from the cached Crossref records); python references/harvest.py doi <DOI> re-checks a record. Python 3 with NumPy and Matplotlib; no other numerical dependencies (pinned versions in requirements.txt). python references/audit_refs.py repeats the reference audit.