Toward transparent rigid packaging from sugarcane bagasse: a consistency-testing framework for nanocellulose–chitosan sheets

Leon Sandler

Independent Researcher, Northbrook, Illinois, USA

ORCID: https://orcid.org/0009-0007-4584-808X

Corresponding author: sandler.leon@gmail.com

Manuscript prepared for submission to Cellulose (Springer). A theoretical and computational study: No experiments were performed, and every output is a screening estimate, not a measured or predicted material property.

# Abstract

Transparent rigid packaging is dominated by fossil-derived polymers, whereas fiber-based packaging is opaque. Dense cellulose nanofibril (CNF) and nanocrystal sheets are transparent as flat films, but whether transparency, wet stiffness and a three-dimensional shape can coexist in one sugarcane-bagasse-derived package has not been established, and one reported attempt to mold transparent CNF objects failed through drying shrinkage. This paper reports no experiments. It applies three consistency screens to a proposed bagasse CNF–chitosan–wax architecture: an optical screen derived from Debye–Bueche scattering theory, a wet-stiffness screen and a geometric forming screen, each propagated through a seeded Monte Carlo analysis over ranges traced to cited literature or explicitly stated assumptions. Under the stated optical-screen assumptions, a 100 µm wall at 10% haze and 5% voids requires a correlation length of about 10 nm or less, and because stiffness fixes a minimum wall thickness, the liquid the package must resist feeds back into the optical budget. Chitosan raises modeled wet stiffness mainly through cross-linking (median gain +1.1 GPa with it, -0.1 GPa without), but its gain in an acidic liquid is small and of uncertain sign. A tray, bowl and cup need total strain tolerances of 0.26, 0.67 and 1.10; no combination of the assumed ranges forms the cup (best case 0.96), which would need a flange wrinkling strain above 0.64. Pass shares depend on the priors, whereas the thresholds, the cup bound and the rank ordering do not. Barrier performance is untested, so every feasibility result is provisional.

Keywords cellulose nanofibrils; transparent nanopaper; chitosan; sugarcane bagasse; thermoforming; consistency testing

# 1 Introduction

Transparent rigid packaging is dominated by polyethylene terephthalate and, increasingly, polylactic acid, chosen largely because they combine clarity, stiffness and liquid tightness. Fiber-based alternatives address material origin; molded pulp, increasingly made from bagasse, wheat and bamboo rather than wood, is an established example (Semple et al. 2022). Fiber-based packaging is opaque, however, and the reason is structural: ordinary paper and cellulose nanopaper consist of the same chemical constituents, and the difference lies in the fiber width and the size of the interstitial cavities that scatter light (Nogi et al. 2009).

Densifying nanofibrils removes that scattering. Films of TEMPO-oxidized cellulose nanofibrils that are only 3–4 nm wide are transparent and flexible (Fukuzumi et al. 2009), and clear nanopapers that are 40 µm thick have been reported to have a total transmittance of 89.3–91.5% and a haze of 4.9–11.7% at a density of 1.29–1.55 g cm−3 (Hsieh et al. 2017). Haze can be tuned by mixing fiber scales (Fang et al. 2014; Yang et al. 2019), and hybrid nanofibril–nanocrystal paper reached a direct transmittance of 75.1% with 10.0% haze, in contrast to 31.1% and 62.0% for earlier nanopaper (Xu et al. 2016). Transparency survives for tens of minutes at 150 °C in flat nanopaper (Nogi et al. 2013), and nanopaper made from sugarcane bagasse nanocrystals has been reported at 91% transmittance and 1.4% haze (Tao et al. 2017). Reviews cover the field (Isogai et al. 2011; Klemm et al. 2011; Moon et al. 2011; Zhu et al. 2014).

Several problems stand between these flat films and a rigid package. Maintaining mechanical properties under hydrated conditions is a recognized and often overlooked challenge for nanocelluloses (Toivonen et al. 2015), and a liquid barrier must be added without reintroducing haze (Lavoine et al. 2012; Azeredo et al. 2017; Hubbe et al. 2017). CNF films are brittle and not thermoplastic, with no clear softening point; thermal roll-to-roll imprinting could pattern them at the micrometer scale only with a softener present (Mäkelä et al. 2016). At the scale of a package the evidence is thinner and more discouraging. Wet molding of CNF mats into three-dimensional objects was feasible, but because of shrinkage during drying none of the formation or drying routes tried yielded transparent and dimensionally stable objects (Rol et al. 2020), and deep drawing of paperboard is regarded as a sensitive process with many failure mechanisms (Hauptmann and Majschak 2011; Vishtal and Retulainen 2012). Nanofibrillation is also energy-intensive (Arvidsson et al. 2015; Kargupta et al. 2022).

The knowledge gap is therefore integration. Each property has been demonstrated mostly on flat films and mostly separately; whether transparency, wet stiffness, barrier performance and a three-dimensional shape can be held together in a single agricultural residue-derived wall has not been established, and the published attempt to form one failed.

This paper asks that question as a consistency test. Each requirement is checked against what the literature supports or against a physical bound, the answer is allowed to be no, and the checks are propagated through the uncertainty that remains. The contribution is the framework and what it returns, not a material: (i) an optical screen whose scattering prefactor is derived from theory rather than fitted, with the haze budget it implies for a wall of given thickness; (ii) a wet-stiffness screen showing what determines whether chitosan helps, including in an acidic liquid; (iii) a forming screen showing that geometry fixes a strain budget independent of the material model; (iv) a ranking of the unknowns that most influence each outcome so that the first measurements are the informative ones; and (v) falsifiable predictions and a validation matrix with numerical thresholds. No experiments were performed. Every parameter is either taken from a cited source or stated as an assumption, and the assumptions are listed in Table 3.

What the combination adds. Each screen alone restates a familiar trend. Three results need the screens together. First, stiffness fixes a minimum wall thickness and thickness fixes the haze, so the liquid the package must resist changes the optical budget (Section 6.6). Second, a wax layer applied before forming must survive the strain the sheet survives, which narrows the forming window of the shallowest geometry (Section 6.8). Third, the joint outcome is set by whichever screen binds, and for deep shapes that is forming, not the optics or the chemistry on which most of the literature concentrates (Section 6.4). The paper also separates what survives a change of prior from what does not (Section 6.7).

# 2 Hypotheses, research questions and status of evidence

Four hypotheses organize the analysis; each is stated so that it can fail.

- H1 (feedstock). Bagasse-derived nanocellulose can form a dense sheet whose void fraction and correlation length meet the haze budget of a rigid wall. It fails if bagasse nanofibril sheets exceed that budget.

H2 (chitosan). Chitosan raises wet stiffness without optical loss, in the liquid the package is meant to hold. It fails if the wet gain is zero or negative in an acidic liquid, or if haze rises.

H3 (barrier). A submicron natural wax layer gives liquid containment without added haze. It is not modeled here and is carried into the validation matrix.

- H4 (forming). The strain budget of the target geometry lies inside the strain the sheet tolerates. It fails for geometries whose budget exceeds the sum of the tolerated tensile and compressive strains.

These map onto five research questions. RQ1 Can densified bagasse-derived nanocellulose plausibly reach the optical properties a transparent wall requires? RQ2 Can chitosan improve wet performance without optical loss? RQ3 Can a thin hydrophobic layer give moisture resistance while preserving transparency? RQ4 What mechanisms limit forming, and which geometries survive them? RQ5 Which measurements are required to decide viability?

Every statement below carries one of four labels. Established means taken from a cited source. Computed means produced by the model in this paper under stated assumptions. Predicted means a falsifiable consequence of the computation. Unvalidated means not tested by anyone to the author’s knowledge. Table 2 applies these labels.

# 3 Proposed material architecture

The architecture (Fig. 1) is the author’s conceptual integration of separately published elements, not a description of existing material. Sugarcane bagasse is fibrillated to nanofibrils, densified into a transparent sheet, combined with chitosan for wet integrity, coated with a thin hydrophobic layer, and formed into a package. Three consistency tests gate the chain: optical after densification, wet-mechanical after chitosan, and forming at the shaping step.

Fig. 1 Proposed processing chain and the three consistency tests that gate it. The diagram is a conceptual integration of separately published elements, not an existing installation.

## 3.1 Bagasse-derived nanocellulose

World sugarcane production was 1,921 Mt in 2022 (FAO 2024). Bagasse is the fibrous residue after juice extraction, produced in very large volumes and traditionally burned for energy (Kabeyi and Olanrewaju 2023; Ndikumana et al. 2025). Its composition, about 42% cellulose, 25% hemicellulose and 20% lignin (Kim and Day 2011), means that delignification and bleaching bear directly on color and haze, and residual lignin has been shown to affect the production and properties of TEMPO-oxidized nanofibrils from partially delignified bagasse (Scopel et al. 2025). Nanocellulose has been isolated from bagasse by several routes (Bhattacharya et al. 2008; Mandal and Chakrabarty 2011); oxidized nanofibrils produced by microfluidization measured 5–80 nm in diameter (Carneiro Pessan et al. 2023), and TEMPO-oxidized bagasse nanofibrils 150–600 nm long have been used to reinforce films (Otenda et al. 2022). Reviews note that nanostructure synthesis from bagasse still lacks high yields and the ability to scale up (Hiranobe et al. 2024). TEMPO-mediated oxidation of native cellulose is the route that gave the thin, uniform nanofibers behind the clear films above (Saito et al. 2007; Fukuzumi et al. 2009), and higher fibril aspect ratios have been reported to give stiffer and more ductile networks (Sellman et al. 2024), which makes the length distribution of bagasse nanofibrils a relevant unknown.

The feedstock evidence is mixed in a way that defines H1. Nanopaper from bagasse nanocrystals is reported at 91% transmittance and 1.4% haze (Tao et al. 2017), so bagasse can give a clear sheet. An agricultural-residue analog prepared as nanofibrils, rice straw, gave films of only 13–42% transmittance (Jiang et al. 2016). No optical data for transparent sheets made from bagasse nanofibrils were found (Supplementary Information S4). The open question is therefore not whether bagasse can give a clear sheet, but whether bagasse nanofibrils, or a hybrid, keep the clarity at the thickness a rigid wall needs, and whether a sheet made of the stiffer, less entangled nanocrystals tolerates forming; the latter is an expectation, not a cited result.

## 3.2 Densified network

Scattering from a fibril and void network falls as the fibril width and the void fraction fall, because refractive-index contrast is then confined to features much smaller than the wavelength (Nogi et al. 2009; Fukuzumi et al. 2013). Haze in clear nanopaper has been attributed to compressed cavities in residual microsized fibers (Hsieh et al. 2017). The thermal stability of flat nanopaper at 150 °C (Nogi et al. 2013) is relevant to hot-liquid service but is not established for a formed wall. Higher strain to failure has been reported for porous nanopaper, 17% at a modulus of 1.4 GPa and 56% porosity (Sehaqui et al. 2011), with large strains attributed to slippage between fibrils (Henriksson et al. 2008); the mechanical property space of nanofibril sheets is reviewed in (Benítez and Walther 2017). Porosity of that order would defeat the haze budget derived below (Table 4), so ductility and clarity pull in opposite directions; this is an inference from the present screens, not a published result.

## 3.3 Chitosan reinforcement

Chitosan chemistry and solubility are reviewed in (Rinaudo 2006; Pillai et al. 2009). Chitosan is water-insoluble but dissolves in acidic solutions (Melro et al. 2021). It is made commercially from shellfish waste, and fungal sources are being explored as an alternative (Ghormade et al. 2017); the regulatory status of any chitosan for food contact is jurisdiction-specific and is not assessed here. Chitosan films are reported to be highly transparent (Sirviö et al. 2021) and neat films have a modulus of 2.3–3.4 GPa with an elongation above 13% (Fernández-Marín et al. 2024). The decisive precedent is physical cross-linking of nanofibrils with chitosan: films of 80/20 CNF/chitosan reached 70–90% transmittance, and when water-soaked retained a strength of 100 MPa, a strain of 28% and a modulus of 4 GPa at 0.5% strain, against 200 MPa and 8% at 50% relative humidity when dry (Toivonen et al. 2015). The mechanism is a pH switch: chitosan is processed dissolved at low pH, then raising the pH reduces its hydration and promotes multivalent interaction with the fibrils. That is also the vulnerability, since the cross-linking depends on a neutral or alkaline environment. A second precedent cuts the other way: adding chitosan lowered the modulus of carrot nanofiber films from 14.71 to 8.76 GPa at 5 wt% (Szymańska-Chargot et al. 2019). Chitosan can therefore help or hurt, and the sign depends on the interface. In the reverse arrangement, with CNF as the filler in chitosan films, tensile properties were optimized at 15 g of CNF per 100 g (Azeredo et al. 2010).

## 3.4 Hydrophobic barrier

A submicron natural wax layer is proposed. Its thickness is far below the scattering scale, so little added haze is expected, but this is inferred. The oxygen and oil barrier properties of microfibrillated cellulose films and coatings (Aulin et al. 2010) and the reactive hydrophobization of CNF films to lower water-vapor permeability (Li et al. 2019) are the closest precedents for barrier function. Hydrophobization of transparent TEMPO-oxidized films has been achieved with alkylketene dimers (Fukuzumi et al. 2009); carnauba wax coatings have water contact angles above 140° on paper, although with nanoparticles and on an opaque substrate (Wang et al. 2017), and ionic cross-linking offers an alternative route to water resistance (Shimizu et al. 2016). A contact angle is not a liquid-holding test, and extended hot or cold containment is untested.

# 4 Evidence status

Table 1 presents the published evidence and the uncertainty that remains for each requirement. Table 2 classifies every claim used here.

Table 1 Published evidence for each requirement of the proposed architecture and what remains uncertain.

| Requirement | Published evidence | Status | Remaining uncertainty |
| --- | --- | --- | --- |
| Transparency, flat film | 89.3–91.5% total transmittance at 40 µm (wood-pulp CNF) (Hsieh et al. 2017); 91% with 1.4% haze from bagasse nanocrystals (Tao et al. 2017) | Established | Bagasse nanofibril sheets; thickness of a rigid wall |
| Low haze | 4.9–11.7% at 40 µm (Hsieh et al. 2017); 10.0% haze, 75.1% direct transmittance, hybrid (Xu et al. 2016) | Established | Haze versus thickness; haze after forming |
| Residue-derived CNF | Rice-straw CNF films 13–42% transmittance (Jiang et al. 2016); bagasse CNF characterized, no clear sheet reported (Otenda et al. 2022; Carneiro Pessan et al. 2023) | Mixed | Whether bagasse CNF meets the haze budget (H1) |
| Thermal stability | Transparency kept after tens of minutes at 150 °C, flat film (Nogi et al. 2013) | Established | Formed wall; hot-liquid service |
| Chitosan transparency | 70–90% transmittance in CNF/chitosan 80/20 (Toivonen et al. 2015) | Established | Haze; other loadings |
| Wet stiffness | Wet 80/20 films: 100 MPa, 28% strain, 4 GPa (Toivonen et al. 2015); chitosan lowered modulus elsewhere (Szymańska-Chargot et al. 2019) | Established, conflicting | Acidic liquids; interface; long exposure (H2) |
| Hydrophobicity | AKD on transparent films (Fukuzumi et al. 2009); wax on opaque paper (Wang et al. 2017) | Precedent only | Transparent wax layer; liquid hold (H3) |
| Forming | Molded CNF objects not transparent or stable (Rol et al. 2020); micropatterning only (Mäkelä et al. 2016) | Negative/absent | Any transparent formed wall (H4) |
| Impact resistance | No evidence found for thin dense nanofibril walls | Unvalidated | Filled-container drop |

Table 2 Classification of the claims used in this paper.

| Label | Examples |
| --- | --- |
| Established (cited) | Transparent, low-haze CNF and CNC nanopaper as flat films; wet-state CNF/chitosan integrity at neutral pH; chitosan dissolves in acid |
| Computed (this work) | Haze budget; angular correction to the cubic law; sign of the chitosan effect; strain budgets and forming windows; Monte Carlo shares and rankings |
| Predicted (this work) | Haze growing with thickness; chitosan benefit lost in acid; forming limited by flange tolerance rather than fracture (Section 8) |
| Assumed | 11 of the 19 parameter ranges (Table 3); the 10% haze and 1 GPa wet-stiffness requirements |
| Unvalidated | Any formed transparent wall; filled-cup drop; liquid containment; lid sealing; life-cycle impact; compostability of the finished structure |

# 5 Screening framework

Three screens test the requirements of Table 1. They are screens in the strict sense: each either implements a physical bound or states a relation whose assumptions are listed, and none is fitted to the paper’s own data.

## 5.1 Test 1: optical

Light scattered by a dense nanofibril network is treated as scattered from refractive index fluctuations in a random two-phase medium, a solid cellulose phase of index nc with air voids of volume fraction φ. In the Born approximation with an exponential correlation function of length a, the framework of Debye and Bueche (Debye and Bueche 1949), applied to random porous solids by Debye, Anderson and Brumberger (Debye et al. 1957), gives a scattering coefficient that depends on the thickness-independent structure alone. The direct (unscattered) fraction of light through a sheet of thickness t is

Td = exp−τ
            t	(1)

and the scattering coefficient, integrated over all angles for unpolarized light, is

τ = K
            fm
            φ1 − φΔε2a3
            gλ4	(2)

where Δε = nc2 − 1 is the permittivity contrast, λ is the vacuum wavelength (550 nm throughout), fm is a morphology factor carrying the uncertainty about the real structure, and K = 64π4/3 ≈ 2.08×103. K is derived and not fitted: it is the small-angle limit of the angular integral of the Debye–Bueche expression multiplied by the polarization factor of unpolarized light. The factor g(a) is the numerically evaluated angular integral relative to that limit and equals 1 when a is much smaller than the wavelength. It matters here. Table S1 of the Supplementary Information gives g(a); in brief, g = 0.97 at 5 nm, 0.90 at 10 nm, 0.69 at 20 nm, 0.37 at 40 nm and 0.14 at 80 nm, so the closed cubic law is accurate to approximately 12% up to 10 nm but overestimates the scattering 7.2 times at 80 nm, the top of the reported bagasse nanofibril range. Haze, defined as transmitted light deviating by more than 2.5° (ASTM International 2021), follows from single scattering as follows:

H = fh1 − e−τte−τt + fh1 − e−τt	(3)

where fh is the fraction of scattered light going forward beyond 2.5°, computed from the same angular integral (0.5 for small features). Surface reflection multiplies direct and diffuse light alike and cancels in the ratio. Eqs. (1)–(3) are valid for τt up to about 1; beyond that, repeated scattering raises the real haze, so values there are optimistic. Three limits should be stated plainly. The core screen represents bulk scattering only: surface roughness and residual fiber fragments, which dominate haze in some nanopapers (Hsieh et al. 2017), are treated only as bounded additions (Section 6.5), and absorption by residual lignin is omitted. The void fraction is derived from film density as φ = 1 − ρf/ρw, which makes it sensitive to the assumed wall density at the percent level. And Eq. (2) is a screening relation: it has not been validated against small-angle scattering from nanocellulose sheets, which is the measurement that would validate it.

## 5.2 Test 2: wet mechanical

The stiffness of a water-saturated CNF/chitosan sheet with a chitosan mass fraction w is screened with a rule of mixtures in which each phase has its own moisture knockdown:

Ewetw = 1 − wψwκCwEC + w
        κHEH	(4)

κCw = κC0 + ξw1 − κC0	(5)

ξw = ξmax1 − exp−ww*	(6)

EC and EH are the dry moduli of the CNF and chitosan phases; κC0 and κH their water-saturated retention; ψ(w) a dry network-efficiency factor that equals 1 at w = 0 and relaxes to a constant ψ with added chitosan, so that disruption of fibril contacts (as in (Szymańska-Chargot et al. 2019)) can be represented; and ξ(w) the gain in CNF-phase retention from physical cross-linking by chitosan (as in (Toivonen et al. 2015)). In an acidic liquid chitosan hydrates, so its own retention falls to a small value and the cross-linking gain is multiplied by a surviving fraction. Eq. (4) is a Voigt-type bound that assumes perfect load sharing, so it is optimistic; interfacial failure and the swelling of chitosan are not otherwise represented. A linear interpolation in hydration h between the dry and saturated states (Supplementary Information S2) gives the chitosan–moisture map of Fig. 3.

## 5.3 Test 3: forming

Forming a flat sheet into a package requires the sheet to supply the surface area of the package. For a frustum container with base diameter db, top diameter dt and depth h, the surface area is

Acup = πdb24 + πdb + dt2h2 + dt − db22	(7)

and the mean equibiaxial strain the sheet would carry if all of that area came from stretching, relative to the base footprint, is the strain budget

εb = 12lnAcupπdb24	(8)

Because the strain is never perfectly uniform, the peak strain is not below this mean, so it is a lower bound on what the sheet must tolerate. Material drawn in from the flange reduces the tensile burden at the cost of compressive strain ln(LDR) at the flange edge, where LDR = D0/db is the limiting draw ratio of a blank of diameter D0. The tensile strain the sheet may carry is limited by fracture or, if it comes first, by the onset of scattering voids, which is lower than fracture whenever the ratio rv of void-onset strain to failure strain is less than one:

εcrit = min1,
            rvεf0 + Δεw
            h	(9)

with εf0 the ambient failure strain, Δεw its gain when water-saturated and h the hydration (0 ambient, 1 saturated). The analogy for εvoid is deformation-induced cavitation and stress whitening in semicrystalline polymers (Lyu et al. 2019); for nanocellulose it is an inference. Tensile strain falls with LDR as ε = εb − ln(LDR), and flange compression is limited by a wrinkling tolerance εwr, so a forming window LDRmin ≤ LDR ≤ LDRmax, with LDRmin = exp(εb − εcrit) and LDRmax = exp(εwr), exists if and only if

εcrit + εwr ≥ εb	(10)

Three reference geometries are used (Table 3 caption): a lid-like tray (base 100 mm, top 120 mm, depth 12 mm), a bowl (100, 150, 50 mm) and a drinking cup (55, 80, 90 mm). Eq. (10) follows exactly from the stated geometry and strain limits; whether a sheet can actually be formed also depends on friction, drying shrinkage (Rol et al. 2020) and temperature, none of which are represented.

## 5.4 Uncertainty propagation

The 19 parameters of the screens are listed with their ranges and bases in Table 3; 8 are informed by a cited source and 11 are assumptions. Each was sampled independently and uniformly, or log-uniformly where the range spans an order of magnitude, for N = 200,000 samples with a fixed seed (20261002). Outputs were summarized by quantiles, by the share of samples meeting a requirement, and by Spearman rank correlation with the output, which identifies which unknown to measure first. The assumed requirements (haze of 5% or 10%, wet stiffness of 0.5, 1 or 2 GPa) are assumptions: transparency in packaging is reported by several nonequivalent measures (Guzman-Puyol et al. 2022), and the package-specific requirement belongs to a design brief, not to this paper.

Table 3 Parameter registry. Status ‘lit’ means that the range is informed by the cited source; ‘assumed’ means that it is the author’s bracket. Sampling is uniform (u) or log-uniform (lu). Reference geometries (base, top, depth in mm): tray 100, 120, 12; bowl 100, 150, 50; cup 55, 80, 90.

| Parameter | Range | Unit | Dist. | Status | Basis |
| --- | --- | --- | --- | --- | --- |
| Film density ρf | 1.29 – 1.55 | g cm−3 | u | lit | Measured density of clear transparent nanopaper, Hsieh et al. 2017 |
| Cell-wall density ρw | 1.5 – 1.6 | g cm−3 | u | assumed | Cell-wall density, amorphous (~1.5) to crystalline (~1.6) cellulose |
| Refractive index nc | 1.5 – 1.62 | - | u | assumed | Refractive index of the cellulose phase; anisotropic, complex index measured for TEMPO-CNF films in Niskanen et al. 2022 |
| Correlation length a, wood-pulp scale | 3 – 15 | nm | lu | lit | Correlation length scale of void structure ~ wood-pulp fibril width: 3-4 nm in Fukuzumi et al. 2009, 3-15 nm in Hsieh et al. 2017 |
| Correlation length a, bagasse range | 5 – 80 | nm | lu | lit | Bagasse CNF diameters 5-80 nm after microfluidization, Carneiro Pessan et al. 2023 |
| Morphology factor fm | 0.3 – 3 | - | lu | assumed | Multiplier on the derived prefactor for departures from exponential correlation and the Born approximation |
| CNF dry modulus EC | 4 – 14 | GPa | u | lit | Dry CNF film modulus: 4.79 GPa Qing et al. 2012; ~4 GPa Jiang et al. 2016; 14.7 GPa Szymańska-Chargot et al. 2019 |
| Chitosan dry modulus EH | 2 – 4 | GPa | u | lit | Neat chitosan film modulus 2.3 and 3.4 GPa, Fernández-Marín et al. 2024 |
| Network efficiency ψ | 0.5 – 1.1 | - | u | lit | Dry network efficiency with chitosan present; 8.76/14.71 = 0.60 at 5 wt% in Szymańska-Chargot et al. 2019, up to ~1 or slightly above if no disruption |
| Plain-CNF wet retention κC0 | 0.02 – 0.5 | - | lu | assumed | Retained fraction of plain-CNF stiffness when water-saturated |
| Chitosan wet retention κH | 0.05 – 0.6 | - | u | assumed | Retained fraction of chitosan stiffness when water-saturated (neutral) |
| Cross-linking gain ξmax | 0 – 0.8 | - | u | assumed | Maximum wet-retention gain from physical cross-linking by chitosan; Toivonen et al. 2015 shows the effect exists (wet films keep 4 GPa) |
| Gain saturation w* | 0.05 – 0.2 | - | u | assumed | Chitosan fraction at which the cross-linking gain saturates |
| Chitosan retention, acid | 0 – 0.1 | - | u | assumed | Chitosan retention in an acidic liquid: chitosan is water-insoluble and dissolves in acidic solutions, Melro et al. 2021 |
| Gain surviving acid | 0 – 0.5 | - | u | assumed | Fraction of the cross-linking gain surviving an acidic liquid |
| Ambient failure strain εf0 | 0.03 – 0.16 | - | u | lit | Failure strain at ambient humidity: 8% at 50% RH Toivonen et al. 2015; 16% Jiang et al. 2016; lower bound assumed for a brittle dense sheet |
| Wet strain gain Δεw | 0.05 – 0.3 | - | u | lit | Failure-strain gain when wet; Toivonen et al. 2015 reports 28% wet vs 8% at 50% RH |
| Void-onset ratio rv | 0.2 – 1 | - | u | assumed | Ratio of microvoid-onset strain to failure strain; <1 means transparency is lost before the sheet fractures |
| Wrinkle tolerance εwr | 0.05 – 0.5 | - | u | assumed | Compressive log-strain the flange tolerates before wrinkling (maximum draw ratio is exp of this value); no value exists for nanocellulose sheets |

## 5.5 Verification and computational methods

A screening model cannot be validated against data it was not built from, so the code is checked against limits known independently of it. The 58 automated verification checks passed; they confirm that the angular integral reduces to its closed form for small features; that Debye–Bueche scattering reduces to the Rayleigh result for dilute small spheres; that the scattered-light fractions conserve energy; that Eq. (2) scales as a3 and as φ(1−φ) in the small-feature limit and more slowly beyond it; that the haze inversion round-trips; that the single-scattering relation maps the direct transmittance and haze pairs reported by Xu et al. (2016) to within 12 percentage points (14.2% against 10% and 52.6% against 62%); that the wet-stiffness screen recovers plain CNF at w = 0, neat chitosan at w = 1 and the rule of mixtures when cross-linking and disruption are switched off; that the forming window opens at the strain budget; that the composite surface-and-bulk slab reduces to Eq. (3) when the additions are zero, that rough-surface scattering reaches its small-roughness limit and that the thickness coupling conserves rigidity; and that every prior scheme stays inside its stated support. These checks show that the code implements the stated relations; they are not experimental validation. All results were produced by one seeded run (Python 3, NumPy); the code is deposited (Data and code availability).

Use of generative AI and handling of evidence. Generative AI (Claude, Anthropic) was used as an assistive tool during manuscript preparation and software development, including code drafting, code review, figure-script drafting, scripts that retrieve literature records, and drafting and language editing of the manuscript text. The author defined the research question, the requirements and the assumptions, directed the computational workflow and the verification criteria, reviewed the interpretation of the literature and approved every scientific conclusion. All computational results were generated by the deposited code and checked against the 58 automated verification checks described above; the author reviewed the outputs. No AI-generated data, references, experimental results or scientific conclusions were accepted without author verification, and the study reports no experimental data. No AI tool is an author. Every reference was resolved against its Crossref record by script, a final audit re-resolved every record and located each quoted number in the cited abstract where one was accessible (Supplementary Information S4), and, for references whose abstract could not be retrieved, the claim attached is limited to what the title states. Statements of absence rest on the documented searches in Supplementary Information S4. The author takes full responsibility for the accuracy, integrity and interpretation of the work.

## 5.6 Bounded extensions

Four bounded extensions test how much the conclusions depend on what the core screens leave out. Every range they use is an assumption (Supplementary Information S7–S10) and none of them enters the 19-parameter registry or the numbers of Sections 6.1–6.4. Surface and coarse scattering. Each film face is treated as a rough interface of RMS height σ. For small slopes, scalar theory gives the fraction of light that one face scatters beyond 2.5° as

sface = fs1 − exp−Φ2,
        Φ = 2πnf − 1σλ	(11)

where nf is the film index and fs the share of that light leaving the cone. This is the Born-type description that relates the texture of a surface to the light it scatters (Jäger and Zeman 2009). A coarse residual population (fiber fragments, aggregates) is added as a second Debye–Bueche term with its own volume fraction and correlation length, bounded so that it is detectable only through its haze. The two faces, the nanofibril network and the coarse term are combined by following the direct and diffuse light through each in turn (Supplementary Information S7); the result reduces to Eq. (3) when the additions are zero. Prior sets. The Monte Carlo analysis is repeated under seven prior schemes (base, uniform, centered, widened, narrowed, optimistic, pessimistic; Supplementary Information S8) to separate results that survive a change of prior from shares that move with it. Thickness coupling. A rigid wall is judged by its flexural rigidity, proportional to E t3 in thin-plate theory. Anchoring the reference requirement (1 GPa at 100 µm), the thinnest wall of equal rigidity is

tmin = trefErefE13	(12)

with tref = 100 µm and Eref = 1 GPa, and the haze is evaluated at tmin. Only the t−3 scaling is physics; the anchor is an assumption. Wax layer. A layer of 0.2–1 µm with its own surface roughness and crystallite scattering is added on one face, and, for coating applied before forming, a cracking strain εwax caps the tolerated tensile strain (Supplementary Information S10). Liquid containment itself is not modeled.

# 6 Results

## 6.1 Optical: a haze budget set by thickness and correlation length

Haze depends on the structure only through φ(1−φ)a3g and on the wall only through its thickness, so a target haze fixes a budget (Fig. 2a). For a 100 µm wall at 5% haze the budget is φ(1−φ)a3 ≤ 22 nm3; at 200 µm it is 11 nm3. Expressed as the largest correlation length for a given void fraction (Table 4), a 100 µm wall at 10% haze and 5% voids needs a ≤ 10.0 nm, and a 200 µm wall at 5% haze and 5% voids needs a ≤ 6.2 nm. The wood-pulp fibril scale (3–15 nm) sits across these thresholds, and the bagasse range (5–80 nm) extends far above them.

Fig. 2 Optical screen. a Haze of a 100 µm wall from bulk scattering as a function of void fraction and correlation length, with the wood-pulp fibril scale (blue box; Hsieh et al. 2017, Fukuzumi et al. 2009) and the extension to the reported bagasse range (orange; Carneiro Pessan et al. 2023); the dashed red curve is the 5% contour for a 200 µm wall. b Haze against thickness for three structures under bulk scattering, with the observed 4.9–11.7% haze of 40 µm clear nanopaper (point) and the gray band showing the opposite limit, in which that haze is surface-dominated and independent of thickness. The region between the two limits is what a thickness series must measure.

Table 4 Largest correlation length a (nm) that keeps the haze of a wall at or below its target by thickness and void fraction φ (full angular integral, nc = 1.55; fm = 1).

| Thickness (µm) | Haze ≤ 5%: φ = 2% | 5% | 10% | Haze ≤ 10%: φ = 2% | 5% | 10% |
| --- | --- | --- | --- | --- | --- | --- |
| 40 | 14.8 | 10.8 | 8.7 | 19.1 | 13.8 | 11.0 |
| 100 | 10.7 | 7.9 | 6.3 | 13.7 | 10.0 | 8.0 |
| 200 | 8.4 | 6.2 | 5.0 | 10.7 | 7.9 | 6.3 |

How well does the screen reproduce published haze? It is not a calibration. With structures drawn from the literature, the bulk-scattering haze of a 40 µm wood-pulp sheet has a median of 1.5% and reaches the observed 4.9–11.7% band in only 14% of samples (73% lie below it and 13% above it) (Hsieh et al. 2017). Bulk void scattering at the nanofibril scale therefore does not by itself explain the haze of published clear nanopaper; surface roughness and residual fiber fragments probably contribute, as the original authors attribute. The most direct consequence is the bracket of Fig. 2b: if the observed haze is mostly bulk, it scales with thickness, and a 100–200 µm wall is far hazier than 40 µm nanopaper, and if it is mostly surface, it does not. Which limit applies is unmeasured and is the first optical measurement; Section 6.5 tests what could close the gap.

Over the sampled ranges (Table 5), a wood-pulp-scale structure meets a 10% haze target at 100 µm in 69% of samples and at 200 µm in 56%; with the bagasse range the shares fall to 26% and 18%. Those shares are conditional on the assumed prior over correlation length, which is uniform on a logarithmic scale, and should be read as a ranking and not as a probability that the material works; for 53% of bagasse samples at 100 µm τt exceeds 1, where the single-scattering estimate is optimistic. The robust results are the thresholds of Table 4. Sensitivity is dominated by the correlation length (Spearman ρ = +0.80 for the bagasse range, +0.74 for the wood-pulp scale), followed by film density (-0.37), as the cubic law implies.

Table 5 Optical screen over the sampled ranges: median haze and the share of samples meeting a haze target, by feedstock range and wall thickness.

| Range | Thickness (µm) | Median haze | Haze ≤ 5% | Haze ≤ 10% | τt > 1 |
| --- | --- | --- | --- | --- | --- |
| Wood-pulp scale | 40 | 1.5% | 73% | 85% | 1% |
| Wood-pulp scale | 100 | 3.7% | 56% | 69% | 6% |
| Wood-pulp scale | 200 | 7.4% | 42% | 56% | 14% |
| Bagasse range | 40 | 27.4% | 28% | 37% | 39% |
| Bagasse range | 100 | 58.6% | 18% | 26% | 53% |
| Bagasse range | 200 | 85.9% | 12% | 18% | 62% |

## 6.2 Wet mechanical: the sign of the chitosan effect

At neutral pH, adding 20% chitosan raises the median modeled wet stiffness from 0.85 to 2.36 GPa (5–95% range 0.69–5.56 GPa), and the share of samples reaching 1 GPa rises from 45% to 88%. In an acidic liquid the gain disappears: the median change is -0.01 GPa, the share reaching 1 GPa is 51%, and chitosan improves wet stiffness in 49% of samples, against 86% at neutral pH (Table 6, Fig. 3a). The effect is therefore not intrinsic to chitosan but depends on the cross-linking and on the liquid. Removing the cross-linking term on the same draws changes the median gain at neutral pH from +1.08 to -0.10 GPa and the share of samples in which chitosan helps from 86% to 35%, so in the screen the benefit is carried by cross-linking, not by the stiffness of the chitosan phase. Wet stiffness is most sensitive to the cross-linking gain ξmax (Spearman ρ = +0.64 for the neutral case), then to the dry CNF modulus (+0.51) and the plain-CNF wet retention (+0.33); in acid the plain-CNF retention dominates (+0.70) because the chitosan contribution is lost.

The screen can be compared with the published wet datum. The reported modulus of 4 GPa for water-soaked 80/20 films (Toivonen et al. 2015) lies at the 82nd percentile of the modeled distribution (18% of samples reach it), so the screen brackets the datum, but its center is conservative relative to it, as expected if the pH-switched processing sits at the favorable end of the cross-linking range. The ratio of 0.60 reported for chitosan-disrupted carrot nanofiber films (Szymańska-Chargot et al. 2019) lies inside the assumed range of the network-efficiency factor. These are consistency checks, not calibrations, and the acid case rests on the assumption, supported by the dissolution of chitosan in acid (Melro et al. 2021) but not by any wet CNF/chitosan measurement in acid, that the cross-linking gain is largely lost.

Fig. 3 Wet-stiffness screen. a Water-saturated stiffness against the chitosan fraction for a neutral and an acidic liquid (median and 5–95% band); the star is the wet datum of Toivonen et al. (2015). b, c Stiffness against the chitosan fraction and hydration at median parameters for the neutral and acidic liquids; contours at 0.5, 1, 2 and 4 GPa. The 20% chitosan column is the only loading with a published wet datum; the rest of each map is extrapolated.

Table 6 Wet-stiffness screen: median water-saturated stiffness, the share of samples reaching 1 GPa (an assumed requirement) and the share in which chitosan increases stiffness above that of plain CNF.

| Chitosan (wt%) | Neutral: median (GPa) | ≥ 1 GPa | Helps | Acidic: median (GPa) | ≥ 1 GPa | Helps |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0.85 | 45% | – | 0.85 | 45% | – |
| 5 | 1.79 | 78% | 86% | 0.99 | 50% | 54% |
| 10 | 2.13 | 85% | 86% | 1.04 | 52% | 53% |
| 20 | 2.36 | 88% | 86% | 1.03 | 51% | 49% |
| 30 | 2.34 | 90% | 84% | 0.96 | 48% | 44% |

## 6.3 Forming: geometry sets the burden

The strain budget of Eq. (8) is 0.262 for the tray, 0.667 for the bowl and 1.105 for the cup, corresponding to surface areas 1.7, 3.8 and 9.1 times the base footprint (Fig. 4a). With no stretching, forming them would need blank-to-punch ratios of 1.30, 1.95 and 3.02. Over the sampled strain tolerances a forming window exists, for saturated forming, in 86% of tray samples, 7% of bowl samples and none of the cup samples (Table 7). Within the assumed ranges the cup result does not depend on the sampling: the largest total tolerance εcrit + εwr reachable anywhere in the assumed ranges is 0.96 for saturated forming, 0.81 at half hydration and 0.66 ambient, all below the cup’s 1.10 (the dashed box of Fig. 4a does not reach the cup line). The bowl is out of reach in the ambient state, where the best case of 0.660 falls just short of the 0.667 needed, and is reached only when the sheet is hydrated (0.81 at half hydration, 0.96 saturated) and at the upper end of the wrinkling tolerance.

Among the unknowns, the wrinkling tolerance of the flange dominated the bowl margin (Spearman ρ = +0.85), followed by the void-onset ratio (+0.39), the wet strain gain (+0.27) and, last, the ambient failure strain (+0.14). When draw-in supplies most of the material, it is the compressive limit that matters, not fracture, which reorders the usual emphasis on strain to failure. At the median tolerances, a straight-walled cup could have a depth of only 0.23 (ambient) to 0.33 (wet) base diameter.

Fig. 4 Forming screen. a Mean tensile strain at the wall against the limiting draw ratio for the three geometries (lines) and the box of tolerated strain at median ambient and wet tolerances (solid) and at the best case over all assumed ranges (dashed); a forming window exists only where a geometry line passes through a box. b Deepest straight-walled cup (depth over base diameter) that a given total tolerance can form, with the equivalent ratio of each geometry (dashed) and the three tolerances.

Table 7 Forming screen: strain budget of each geometry and the share of samples with a forming window by forming hydration.

| Geometry | Strain budget | Area ratio | Ambient | Half hydration | Saturated |
| --- | --- | --- | --- | --- | --- |
| Tray (lid-like) | 0.262 | 1.7 | 65.9% | 77.3% | 85.5% |
| Bowl | 0.667 | 3.8 | 0.0% | 1.2% | 6.9% |
| Cup | 1.105 | 9.1 | 0.0% | 0.0% | 0.0% |

## 6.4 Integration

For a reference design (100 µm wall, 20% chitosan, haze ≤ 10%, wet stiffness ≥ 1 GPa, forming at saturation) the share of sampled designs passing all three tests is 52% for a tray with a wood-pulp-scale structure and a neutral liquid, 19% with a bagasse-range structure, and 30% and 11% in an acidic liquid; for a bowl it is 4% and 2%, and for the cup it is zero in every case (Fig. 5a). These shares depend on the assumed ranges and are reported to rank the cases. The conclusions that do not depend on them are the thresholds of Table 4, the bound on the cup, and the order of the unknowns in Fig. 5b; Section 6.7 tests them under alternative priors.

Fig. 5 Integration. a Share of sampled designs passing all three tests at the reference design (100 µm wall, 20% chitosan, haze ≤ 10%, wet stiffness ≥ 1 GPa, forming at saturation), by geometry, feedstock range and liquid. Shares depend on the assumed ranges; the zero for the cup holds within the assumed range (in the best case, 0.96 < 1.10). b Spearman rank correlation of the leading unknowns with the optical, wet-mechanical and forming outputs: the quantities to measure first.

## 6.5 Optical-model validation: what could close the gap

Section 6.1 reported that bulk scattering by the nanofibril network reproduces the observed haze of clear nanopaper in only 14% of samples. Two additions were tested (Section 5.6). Surface scattering on its own would need an RMS height of 28–44 nm on each of two faces to give the observed 4.9–11.7% haze (67 nm if only 30% of the scattered light leaves the 2.5° cone), several times the 3–15 nm fibril width, so the faces would be rougher than the fibrils that form them; atomic-force or optical profilometry of the faces is the measurement that decides. Over the assumed roughness range (1–30 nm) the median haze of a 40 µm wood-pulp-scale sheet rises from 1.5% to 2.3%, and the share inside the observed band from 14% to 17%. A coarse population of volume fraction 0.001–0.03% and size 50–300 nm acts more strongly: the median rises to 3.8% and the share inside the band to 25%. With both, the median is 4.6% and 29% of samples lie inside the band, but 53% still lie below it (Table 8, Fig. 6a). The additions narrow the gap and do not close it, so the bulk screen remains a lower bound on haze, and the observed 4.9–11.7% is most simply explained by a small population of coarse scatterers that no density measurement would reveal.

Table 8 Haze of a wood-pulp-scale sheet with the bulk screen alone and with the bounded additions: median haze, and the share of samples inside and below the observed 4.9–11.7% band at 40 µm.

| Scattering included | Median haze 40 µm | Inside band | Below band | Median haze 100 µm | Median haze 200 µm |
| --- | --- | --- | --- | --- | --- |
| Nanofibril bulk only (core screen) | 1.5% | 14% | 73% | 3.6% | 7.3% |
| + rough surfaces | 2.3% | 17% | 69% | 4.5% | 8.0% |
| + coarse population | 3.8% | 25% | 58% | 9.4% | 18.1% |
| + both | 4.6% | 29% | 53% | 10.0% | 18.7% |

Consequences for the optical budget. The coarse-population explanation has a design consequence that no single-thickness measurement reveals. A population that alone gives 8% haze at 40 µm (volume fraction 0.054% at 100 nm, 0.015% at 300 nm) would give 19% haze at 100 µm and 34% at 200 µm regardless of the nanofibril scale because haze then increases with thickness. The correlation-length threshold of Table 4 is therefore a necessary condition under the bulk model, not a sufficient one: it holds only if the coarse population is controlled. The threshold itself is slightly changed by surface roughness (for 100 µm, 10% haze and 5% voids, a ≤ 10.0 nm with none, 9.8 nm at 10 nm RMS and 9.0 nm at 20 nm RMS) or by a small coarse population (9.4 nm at 0.005%). The thickness series of P1 (Section 8) separates these cases, since surface haze is independent of thickness and coarse-population haze is not.

Fig. 6 Optical-model validation and the coupled window. a Cumulative distribution of the haze of a 40 µm wood-pulp-scale sheet for the bulk screen alone and with rough surfaces and a coarse population added (assumed ranges, Supplementary Table S10); the green band is the observed 4.9–11.7%. b Haze budget (maximum correlation length at 5% voids) against thickness for 10% (solid) and 5% (dashed) haze, with the minimum thickness that stiffness requires at the median wet modulus for a neutral and an acidic liquid (lines; bands are in the 5–95% range). A design must lie to the left of the budget curve and above the line.

## 6.6 Thickness couples the optical and stiffness screens

Equation (12) makes thickness the variable that joins the screens: stiffness sets the thinnest wall that is rigid enough, and the haze budget sets the finest structure that wall may carry. At the median wet modulus the minimum thickness is 75 µm for a neutral liquid (5–95% range 56–113 µm) and 99 µm for an acidic one (68–160 µm), so the liquid the package must resist changes the optical budget: the allowed correlation length at 5% voids and 10% haze is 11.1 nm for the neutral and 10.0 nm for the acidic case (Fig. 6b). With each sample’s own modulus setting its own thickness, a wood-pulp-scale structure meets the 10% haze target in 74% of samples for a neutral liquid and 69% for an acidic one, and a bagasse-range structure in 29% and 26%; evaluated at the fixed 100 µm of Section 6.4 and also required to reach 1 GPa, the shares are 61% and 36% for the wood-pulp scale and 23% and 13% for the bagasse range. The coupling does not rescue the bagasse range, but it shows that the stiffness result and the optical result cannot be quoted at a common thickness without choosing one.

## 6.7 Robustness to the prior distributions

Eleven of the nineteen ranges are assumptions, so the Monte Carlo shares were recomputed under seven prior schemes (Section 5.6). The shares move by tens of percentage points (Table 9, Fig. 7): the share of wood-pulp-scale structures meeting the haze target at 100 µm ranges from 46% to 80% and that of the bagasse range from 2% to 35%, the tray’s forming window from 65% to 99%, the bowl’s from 0.3% to 27.5%, and the joint pass share of the tray from 25% to 78%. They are not results about the material. Four statements survive every scheme: the tray has a larger window than the bowl and the bowl a larger one than the cup (yes); the wood-pulp scale beats the bagasse range optically (yes); chitosan helps in more samples at neutral pH than in acid (yes); and the median chitosan gain is smaller in acid than at neutral pH (yes). Two statements are conditional. The sign of the median chitosan gain in acid is not fixed: it runs from -0.36 to +0.17 GPa across the schemes, against +0.56 to +1.46 GPa at neutral pH, so the defensible statement is that the gain is small and of uncertain sign in acid. And the cup is closed in every scheme except the widened one, where the upper bound of the wrinkling tolerance rises from 0.50 to 0.72 and the best-case total tolerance to 1.19, above the cup’s 1.10; there 0.015% of samples form it.

Table 9 Headline shares under seven prior schemes (base, uniform, centered, widened, narrowed, optimistic, pessimistic): the base value, the range across schemes and the schemes that give its extremes.

| Output | Base | Lowest | Highest | Lowest in | Highest in |
| --- | --- | --- | --- | --- | --- |
| Optical pass, wood-pulp scale, 100 µm | 69% | 46% | 80% | uniform | optimistic |
| Optical pass, bagasse range, 100 µm | 26% | 2% | 35% | centered | optimistic |
| Chitosan helps, neutral | 86% | 70% | 99% | uniform | narrowed |
| Chitosan helps, acidic | 49% | 26% | 63% | uniform | widened |
| Forming window, tray | 85% | 65% | 99% | pessimistic | narrowed |
| Forming window, bowl | 7.0% | 0.3% | 27.5% | narrowed | widened |
| Forming window, cup | 0.00% | 0.00% | 0.02% | all other schemes | widened |
| All three pass, tray (wood-pulp) | 53% | 25% | 78% | pessimistic | optimistic |
| All three pass, bowl (wood-pulp) | 4.3% | 0.2% | 16.9% | narrowed | widened |
| Median acid gain (GPa) | -0.01 | -0.36 | +0.17 | uniform | widened |

Fig. 7 Robustness to prior distributions. Each row is a headline share; the bar spans the seven prior schemes, and each marker is one scheme. The order of the rows within a pair (tray, bowl and cup; wood-pulp scale and bagasse range; neutral and acidic) is the same in every scheme.

What the cup needs. The closed cup is the result most worth stating as a requirement. Even with every tensile tolerance in its best case (0.46 for a saturated sheet), the flange would have to tolerate a wrinkling strain of 0.64, that is, a limiting draw ratio of 1.91, against an assumed upper bound of 0.50 (1.65). At the median tensile tolerance (0.15), the requirement is 0.96, and the draw ratio is 2.60. The conclusion is thus not that a cup cannot be drawn but that it needs a flange wrinkling tolerance well beyond anything assumed here, for which no measurement on nanocellulose sheets exists.

## 6.8 Barrier layer: a bounded test of H3

The wax layer of H3 is not part of the integrated screens, and liquid containment is untested. Its effect on the other two requirements can nevertheless be bounded (Section 5.6). Optically, the assumption that a submicron layer adds no haze is not safe: over the assumed ranges a layer on one face of a 100 µm wall adds a median of 1.0 haze points (5–95% range 0.1–4.8), more than one point in 51% of samples, more than two in 28% and more than five in 4%. Surface roughness of the wax (Spearman ρ = +0.56), the index contrast of its crystallites (+0.45) and their size (+0.38) drive it. Mechanically, a coating applied before forming must survive the same strain as the sheet. With a cracking strain of 1–10% the share of tray samples with a forming window at saturation falls from 86% to 65%, and the bowl’s from 6.9% to 0.0%; coating after forming avoids this and moves the burden to conformal coating of a formed wall. These are sensitivities to assumed ranges. They classify every feasibility result in this paper as provisional, because the liquid-holding function that the coating exists to provide has not been tested, and they turn H3 from an inference of ‘no added haze’ into a measurable threshold: an added haze of at most one point.

Table 10 Bounded sensitivity of the wax layer (assumed ranges): added haze at 100 µm and the share of samples with a forming window at saturation, uncoated and coated before forming.

| Quantity | Result |
| --- | --- |
| Added haze, median (5–95%) | 1.0 points (0.1–4.8) |
| Share adding > 1, > 2, > 5 points | 51%, 28%, 4% |
| Median added haze: surface only, crystallites only | 0.21, 0.47 points |
| Tray window: uncoated, coated before forming | 85.5%, 64.9% |
| Bowl window: uncoated, coated before forming | 6.9%, 0.0% |
| Cup window: uncoated, coated before forming | 0.0%, 0.0% |

# 7 Discussion

What the three screens return. The optical screen shows that thickness and correlation length, not material identity, decide whether a dense nanofibril wall is clear: the same structure that gives single-digit haze at 40 µm can be several times hazier at 100–200 µm if scattering is bulk. The wet screen shows that chitosan is a cross-linker whose benefit is conditional on the liquid, not a reinforcement in the ordinary sense. The forming screen shows that, for deep geometries, the sheet would need to supply many times its footprint area, which no tolerance within the assumed ranges provides.

What only the combination returns. Each screen alone restates a familiar trend: smaller features scatter less, chitosan can cross-link nanofibrils, deeper shapes need more strain. Table 11 lists the results that need the screens taken together, and what would be missed if one screen were used alone.

Table 11 Results that require two or more screens and what a single screen would miss.

| Result | Screens combined | What a single screen misses |
| --- | --- | --- |
| The liquid changes the optical budget: median minimum thickness 75 µm (neutral) against 99 µm (acidic), allowed correlation length 11.1 against 10.0 nm (Section 6.6) | Wet stiffness and optical | Each fixes the thickness at 100 µm and cannot see the coupling |
| A wax layer applied before forming narrows the tray window from 86% to 65% and closes the bowl (Section 6.8) | Barrier and forming | The forming screen assumes a bare sheet |
| The correlation-length threshold is necessary, not sufficient: coarse scatterers that explain the observed 40 µm haze give approximately 19% at 100 µm (Section 6.5) | Optical and published haze data | The bulk model alone, or haze at a single thickness |
| Flange wrinkling tolerance, not fracture strain, decides the bowl (Spearman ρ = +0.85), and the cup needs a wrinkling strain above 0.64 | Forming and void-onset limit | Tensile-strain data alone |
| Thresholds, orderings and the cup bound survive seven prior schemes; pass shares do not (Section 6.7) | All three and the prior sets | A single Monte Carlo run |

Scope of the forming result. The cup result applies to forming a flat, dense sheet by drawing, with the strain limits assumed here; it is not universally impossible. Routes that change the burden include multistage drawing with intermediate drying; hydration beyond the saturated state; redistribution of thickness toward the wall, which the uniform-strain budget (a lower bound, Eq. 8) does not capture; storing areas in folds, pleats or a seam instead of strain; and direct molding from a suspension, the route of Rol et al. (2020), which avoids sheet strain at the price of the drying shrinkage that defeated it. None of these is modeled. Each is a candidate whose own limit would need its own measurement, and the framework states the corresponding requirement for the drawing route: a flange wrinkling tolerance above 0.64 for the cup.

Consistency with prior art. The forming result agrees with the one reported attempt at three-dimensional CNF objects, which produced objects by wet molding but not transparent or dimensionally stable ones because of drying shrinkage (Rol et al. 2020). The two findings are complementary: that study identifies a route-specific failure, shrinkage on drying, which this screen does not represent, while this analysis shows a geometric limit that applies whatever the route. The wet-state result is consistent with a pH-switched cross-linking mechanism (Toivonen et al. 2015), and the limits of the closed cubic law matter for the coarse end of the bagasse nanofibril range.

Design implications. The results do not say that a transparent bagasse package is impossible; they say what would have to be true. Shallow geometries such as lids and trays are the only ones inside the assumed tolerances. A cup-like container would need a construction that does not stretch a flat sheet, for example, a wall formed from a flat blank by wrapping with a seam, which trades the strain constraint for seam, leak and optical continuity requirements that are not analyzed here; a transparent window in an otherwise opaque molded-pulp body is another option. Reducing the wall thickness relaxes the optical budget in proportion but decreases stiffness and increases sensitivity to surface defects.

What to measure first. The rankings give an order. For optics, the correlation length and void fraction of a dense bagasse sheet by small-angle X-ray scattering, since the Debye–Bueche form is the one with which such data are analyzed (Debye et al. 1957), followed by haze against thickness. For wet stiffness, the cross-linking gain and the plain-CNF wet retention, including in acidic liquids. For forming, the flange wrinkling tolerance and the strain at which haze first rises.

Relation to CNF and CNC. Nanocrystal sheets from bagasse have given the clearest reported result (Tao et al. 2017), but their stiffness and expected brittleness bear on forming in a way the present screens treat only through the assumed strain tolerances. A hybrid that keeps the clarity of crystals and the entanglement of fibrils, as in Xu et al. (2016), is a natural candidate for H1 and is accommodated by the framework through the structural parameters.

# 8 Falsifiable predictions and validation matrix

Each prediction below follows from the computation and can be shown wrong by a stated measurement.

P1 (thickness scaling). If bulk scattering dominates, haze of a dense nanofibril sheet rises approximately in proportion to thickness between 40 and 200 µm (H ≈ fhτt for τt ≲ 0.3); if surface scattering dominates, haze is nearly independent of thickness. A thickness series decides which, and measured haze outside the bracket of Fig. 2b falsifies the screen.

- P2 (structure predicts haze). Small-angle scattering of the sheet should give φ(1−φ)a3 and a Debye–Bueche correlation length that predict the measured bulk haze within the factor spanned by fm (0.3–3).

- P3 (bagasse threshold). A dense bagasse nanofibril sheet meets a 10% haze target at 100 µm only if its correlation length is less than approximately 10 nm at 5% voids (14 nm at 2%).

P4 (acid reversal). The wet-stiffness gain from 20% chitosan measured after soaking in an acidic liquid is much smaller than after soaking in neutral water, and may be negative; a gain retained in acid falsifies the assumed loss of cross-linking.

- P5 (forming limit). Haze increases before fracture during forming if rv < 1, and a flat dense sheet cannot be formed into the cup geometry by drawing alone; a transparent formed cup falsifies the bound of Eq. (10).

P6 (what scatters). If a small coarse population explains the haze of clear nanopaper, haze rises with thickness (about 19% at 100 µm for a population that gives 8% at 40 µm) and the population is visible by microscopy or wide-angle scattering; if instead the faces scatter, haze is independent of thickness and the RMS height of the faces is tens of nanometers (2.6% haze at 20 nm, 5.7% at 30 nm from two faces).

P7 (wax haze). A submicron wax layer adds measurable haze: in the bounded analysis it adds more than one point at 100 µm in 51% of sampled structures, and a coating that adds at most one point needs smooth, fine-crystalline wax.

Table 12 Validation matrix: the measurement, the threshold derived here and what would falsify it.

| Requirement | Measurement | Threshold derived here | Falsified if |
| --- | --- | --- | --- |
| Bulk scattering | Small-angle X-ray scattering, Debye–Bueche analysis of dense bagasse sheets | φ(1−φ)a3 ≤ 22 nm3 at 100 µm, 5% haze | Measured value exceeds it with haze still low |
| Thickness scaling | Haze (ASTM D1003) at 40, 100, 200 µm | Haze ∝ t (bulk) or constant (surface) | Outside the bracket of Fig. 2b |
| Surface or coarse scatterers | Profilometry of both faces; microscopy or wide-angle scattering of the bulk | Two-face haze 0.7% at 10 nm RMS, 5.7% at 30 nm; coarse volume fraction ≤ 0.054% at 100 nm | Observed haze unexplained by either |
| Feedstock (H1) | Correlation length, bagasse versus wood-pulp CNF at equal density | a ≤ 10 nm at 5% voids (100 µm, 10% haze) | Larger a with haze still within target |
| Wet stiffness (H2) | Wet tensile modulus at 0, 10, 20, 30 wt% chitosan in neutral water | ≥ 1 GPa; model median 2.4 GPa at 20% | Below 1 GPa, or no gain over plain CNF |
| Acid exposure (H2) | Wet modulus after soaking in acidic liquids | Gain over plain CNF near zero (model median -0.01 GPa) | Gain retained in acid |
| Barrier (H3) | Liquid-hold test, haze after coating, abrasion-induced haze | 24 h hold (proposed); added haze ≤ 1 point (exceeded in 51% of the bounded samples) | Leak, or coating adds more than one point |
| Strain tolerance (H4) | Wet and ambient strain to failure; in situ haze against strain | Total tolerance ≥ 0.26 (tray), 0.67 (bowl) | Below the budget of the target geometry |
| Flange wrinkling (H4) | Draw test with blank holder, LDR at wrinkle onset | LDRmax = exp(εwr); needed 1.30 (tray) | LDRmax below the requirement |
| Package | Filled-container drop, lid attachment, thermal cycling | 1 m drop (proposed) | Failure |

The staged program that would test these is: Phase I, material (fibril width, density, small-angle scattering, haze against thickness, with and without delignification); Phase II, composite (chitosan at 0, 5, 10, 20 and 30 wt%, transparency, dry and wet tensile properties in neutral and acidic liquids); Phase III, barrier (contact angle, liquid hold, durability, abrasion-induced haze); Phase IV, forming (shallow, intermediate and full-depth draw; haze, cracking and delamination); Phase V, package (filled-cup drop, extended containment, lid attachment, thermal cycling). Details are in Supplementary Information S6.

# 9 Sustainability and scalability

The constituents (cellulose, chitosan and natural wax) were chosen for potential compatibility with compostability pathways; compostability of the finished structure is unvalidated, and no life-cycle assessment has been performed. Nanofibrillation energy depends on the processing method (Spence et al. 2011) and production routes are reviewed in (Nechyporchuk et al. 2016); refining alone reached a plateau of barrier properties only after 1,800–12,000 kWh t−1 depending on the refiner (Kargupta et al. 2022), and complete defibrillation of rice straw by aqueous counter collision was reported at 15 kWh kg−1 (Jiang et al. 2016). These figures come from different feedstocks, equipment and end points and are not comparable. Life-cycle impact of nanofibril production depends strongly on the pretreatment route and on the electricity mix (Arvidsson et al. 2015), and the scale-up of nanostructures from bagasse remains a stated challenge (Hiranobe et al. 2024). Repulpability of a deliberately void-free sheet is a testable hypothesis, not a result.

# 10 Limitations

- No sheet or package was made or tested. Eleven of the nineteen parameter ranges are assumptions, and every share quoted in Section 6 is conditional on them; the thresholds and the cup bound are the results that depend least on them, and Section 6.7 tests the dependence under six alternative prior sets.

- The core optical screen represents bulk scattering; surface and coarse scattering enter only as bounded additions with assumed ranges (Section 6.5). Absorption by residual lignin, multiple scattering beyond τt of approximately 1 and the anisotropy of cellulose are not represented, and Eq. (2) has not been validated against small-angle scattering from nanocellulose sheets. It does not by itself reproduce the haze of published clear nanopaper. The Born approximation is comfortable at the wood-pulp fibril scale but marginal for correlation lengths of tens of nanometers, where the phase shift across one correlation length reaches 0.25 at 40 nm and 0.50 at 80 nm (Supplementary Table S1).

- The wet-stiffness screen is a Voigt-type bound with an assumed cross-linking term, and its acid case rests on an assumption that is plausible but untested for CNF/chitosan sheets. Interfacial failure, creep and swelling are not represented.

- The forming screen bounds mean area strain and tolerance. Friction, nonuniform thinning, temperature, drying shrinkage (the failure route reported by Rol et al. 2020) and the strain state of the wall are not represented; the wrinkling tolerance is not reported for nanocellulose sheets.

- The thickness coupling rests on an assumed equal-rigidity anchor (1 GPa at 100 µm), and the forming screen treats the drawing of a flat sheet; other routes (multistage or wet forming, folds and seams, direct molding from suspension) are neither modeled nor excluded.

- Liquid containment (H3) is not modeled: only the optical and forming effects of a wax layer are bounded (Section 6.8), with assumed ranges, so every feasibility result is provisional until a liquid-holding test exists. A contact angle is not a liquid-holding test.

Food-contact regulatory status of chitosan, waxes and any additives, compostability and life-cycle impact are not assessed. Some references were available to the verification process only by title, and the claims attached to them are limited accordingly.

# 11 Conclusions

The literature supports each ingredient of a transparent, bagasse-derived nanocellulose–chitosan package for flat films, and it records one failure at the package scale. Three consistency screens show what would have to be true for the ingredients to coexist. A dense wall is clear only if its void fraction and correlation length lie inside a budget set by its thickness: for 100 µm, 10% haze and 5% voids, a correlation length of about 10 nm or less, a threshold the reported bagasse nanofibril range straddles. Chitosan raises wet stiffness mainly through cross-linking, and in the screen that benefit is small and of uncertain sign in an acidic liquid. And geometry sets a strain budget of 0.26, 0.67 and 1.10 for a tray, a bowl and a cup, of which only the tray lies within the assumed tolerances, while the cup lies outside every combination of them unless the flange tolerates a wrinkling strain above 0.64. Stiffness, through wall thickness, couples the liquid to the optical budget, and a wax layer applied before forming narrows the forming window. These are conditional results from stated assumptions. They define the measurements, ranked by influence, that would confirm or falsify the concept, and they locate the binding constraint, forming, in geometry and not only in the material.

# Declarations

Funding This research received no specific grant from funding agencies in the public, commercial or not-for-profit sectors.

Competing interests The author declares that there are no competing financial or nonfinancial interests.

Ethics approval and consent to participate Not applicable. This is a theoretical and computational study with no human participants, human data, animals or experiments.

Consent for publication Not applicable.

Data availability No experimental data were generated in this study. The computational code, the parameter registry (Table 3 and Supplementary Table S10), the fixed random seed (20261002), the Monte Carlo outputs (code/results.json), the verification tests, the figure-generation scripts, the numerical tables underlying Figures 2–7 (code/figure_data), the reference-audit tooling and the log of literature searches are available in a public repository at https://github.com/sandlerleon/bagasse-cnf-chitosan-framework (MIT license for code, CC BY 4.0 for the manuscript files) and are archived on Zenodo, https://doi.org/10.5281/zenodo.23111544, which always resolves to the latest version. The repository contains the software versions (requirements.txt) and the commands that reproduce every reported number; all the results are produced by one seeded run of code/run_analysis.py. The literature-derived parameters are listed individually in Table 3 and the corresponding references. This manuscript and its Supplementary Information are archived as a preprint on Zenodo, https://doi.org/10.5281/zenodo.23111546.

Author contributions Leon Sandler conceived the study, specified the physical model and its assumptions, directed the literature work and the computation, analyzed the results, and reviewed, edited and approved the manuscript.

Use of generative AI Generative AI (Claude, Anthropic) was used as an assistive tool for code drafting, code review, figure-script drafting, literature-record retrieval scripts, and drafting and language editing of the manuscript text. The author defined the research question, requirements and assumptions, directed the workflow and verification, reviewed the literature interpretation and approved all conclusions, and takes full responsibility for the work. No AI-generated data, references or conclusions were accepted without author verification (Section 5.5).

# Appendix: nomenclature

| Symbol | Definition | Unit |
| --- | --- | --- |
| Td | Direct (unscattered) fraction of transmitted light | – |
| τ | Scattering coefficient | m−1 |
| H | Haze: transmitted light deviating by more than 2.5° | – |
| φ | Void volume fraction | – |
| a | Correlation length of the void structure | nm |
| nc | Refractive index of the cellulose phase | – |
| Δε | Permittivity contrast, nc2 − 1 | – |
| λ | Vacuum wavelength (550 nm) | nm |
| t | Wall thickness | µm |
| K | Derived prefactor, 64π4/3 | – |
| fm | Morphology factor | – |
| g | Angular correction to the cubic law | – |
| fh | Forward-scattered fraction beyond 2.5° | – |
| w | Chitosan mass fraction | – |
| Ewet | Water-saturated stiffness | GPa |
| EC, EH | Dry moduli of the CNF and chitosan phases | GPa |
| ψ | Dry network-efficiency factor | – |
| κC0, κH | Water-saturated retention of CNF and chitosan stiffness | – |
| ξ | Gain in CNF-phase retention from cross-linking | – |
| db, dt, h | Base diameter, top diameter and depth of the container | mm |
| Acup | Surface area of the container | mm2 |
| εb | Strain budget (mean equibiaxial log-strain) | – |
| εcrit | Tolerated tensile strain, min(failure, void onset) | – |
| rv | Ratio of void-onset strain to failure strain | – |
| εwr | Tolerated compressive (wrinkling) log-strain | – |
| LDR | Limiting draw ratio, D0/db | – |
| h (hydration) | Hydration, 0 ambient to 1 saturated | – |

# References

Arvidsson R, Nguyen D, Svanström M (2015) Life cycle assessment of cellulose nanofibrils production by mechanical treatment and two different pretreatment processes. Environ Sci Technol 49:6881–6890. https://doi.org/10.1021/acs.est.5b00888

ASTM International (2021) ASTM D1003-21: standard test method for haze and luminous transmittance of transparent plastics. ASTM International, West Conshohocken, PA. https://doi.org/10.1520/D1003-21

Aulin C, Gällstedt M, Lindström T (2010) Oxygen and oil barrier properties of microfibrillated cellulose films and coatings. Cellulose 17:559–574. https://doi.org/10.1007/s10570-009-9393-y

Azeredo HM, Mattoso LHC, Avena‐Bustillos RJ et al (2010) Nanocellulose reinforced chitosan composite films as affected by nanofiller loading and plasticizer content. J Food Sci 75(1). https://doi.org/10.1111/j.1750-3841.2009.01386.x

Azeredo HM, Rosa MF, Mattoso LHC (2017) Nanocellulose in bio-based food packaging applications. Ind Crops Prod 97:664–671. https://doi.org/10.1016/j.indcrop.2016.03.013

Benítez AJ, Walther A (2017) Cellulose nanofibril nanopapers and bioinspired nanocomposites: a review to understand the mechanical property space. J Mater Chem A 5:16003–16024. https://doi.org/10.1039/c7ta02006f

Bhattacharya D, Germinario LT, Winter WT (2008) Isolation, preparation and characterization of cellulose microfibers obtained from bagasse. Carbohydr Polym 73:371–377. https://doi.org/10.1016/j.carbpol.2007.12.005

Carneiro Pessan C, Silva Bernardes J, Bettini SH et al (2023) Oxidized cellulose nanofibers from sugarcane bagasse obtained by microfluidization: Morphology and rheological behavior. Carbohydr Polym 304:120505. https://doi.org/10.1016/j.carbpol.2022.120505

Debye P, Bueche AM (1949) Scattering by an inhomogeneous solid. J Appl Phys 20:518–525. https://doi.org/10.1063/1.1698419

Debye P, Anderson HR, Brumberger H (1957) Scattering by an inhomogeneous solid. II. The correlation function and its application. J Appl Phys 28:679–683. https://doi.org/10.1063/1.1722830

Fang Z, Zhu H, Bao W et al (2014) Highly transparent paper with tunable haze for green electronics. Energy Environ Sci 7:3313–3319. https://doi.org/10.1039/c4ee02236j

FAO (2024) FAOSTAT: crops and livestock products, sugar cane (item 156), production quantity (element 5510), world total. Food and Agriculture Organization of the United Nations, Rome. https://www.fao.org/faostat/. Accessed via Our World in Data, 2 October 2026

Fernández-Marín R, Morales A, Erdocia X et al (2024) Chitosan–chitin nanocrystal films from lobster and spider crab: properties and environmental sustainability. ACS Sustain Chem Eng 12:10363–10375. https://doi.org/10.1021/acssuschemeng.4c01205

Fukuzumi H, Saito T, Iwata T et al (2009) Transparent and high gas barrier films of cellulose nanofibers prepared by TEMPO-mediated oxidation. Biomacromolecules 10:162–165. https://doi.org/10.1021/bm801065u

Fukuzumi H, Saito T, Isogai A (2013) Influence of TEMPO-oxidized cellulose nanofibril length on film properties. Carbohydr Polym 93:172–177. https://doi.org/10.1016/j.carbpol.2012.04.069

Ghormade V, Pathan E, Deshpande M (2017) Can fungi compete with marine sources for chitosan production? Int J Biol Macromol 104:1415–1421. https://doi.org/10.1016/j.ijbiomac.2017.01.112

Guzman-Puyol S, Benítez JJ, Heredia-Guerrero JA (2022) Transparency of polymeric food packaging materials. Food Res Int 161:111792. https://doi.org/10.1016/j.foodres.2022.111792

Hauptmann M, Majschak J (2011) New quality level of packaging components from paperboard through technology improvement in 3D forming. Packag Technol Sci 24:419–432. https://doi.org/10.1002/pts.941

Henriksson M, Berglund LA, Isaksson P et al (2008) Cellulose nanopaper structures of high toughness. Biomacromolecules 9:1579–1585. https://doi.org/10.1021/bm800038n

Hiranobe CT, Gomes AS, Paiva FFG et al (2024) Sugarcane bagasse: challenges and opportunities for waste recycling. Clean Technol 6:662–699. https://doi.org/10.3390/cleantechnol6020035

Hsieh M-C, Koga H, Suganuma K et al (2017) Hazy transparent cellulose nanopaper. Sci Rep 7:41590. https://doi.org/10.1038/srep41590

Hubbe MA, Ferrer A, Tyagi P et al (2017) Nanocellulose in thin films, coatings, and plies for packaging applications: a review. BioResources 12:2143–2233. https://doi.org/10.15376/biores.12.1.hubbe

Isogai A, Saito T, Fukuzumi H (2011) TEMPO-oxidized cellulose nanofibers. Nanoscale 3:71–85. https://doi.org/10.1039/c0nr00583e

Jiang F, Kondo T, Hsieh Y-L (2016) Rice straw cellulose nanofibrils via aqueous counter collision and differential centrifugation and their self-assembled structures. ACS Sustain Chem Eng 4:1697–1706. https://doi.org/10.1021/acssuschemeng.5b01653

Jäger K, Zeman M (2009) A scattering model for surface-textured thin films. Appl Phys Lett 95:171108. https://doi.org/10.1063/1.3254239

Kabeyi MJB, Olanrewaju OA (2023) Bagasse electricity potential of conventional sugarcane factories. J Energy 2023:1–25. https://doi.org/10.1155/2023/5749122

Kargupta W, Seifert R, Martinez M et al (2022) Preparation and benchmarking of novel cellulose nanopaper. Cellulose 29:4393–4411. https://doi.org/10.1007/s10570-022-04563-0

Kim M, Day DF (2011) Composition of sugar cane, energy cane, and sweet sorghum suitable for ethanol production at Louisiana sugar mills. J Ind Microbiol Biotechnol 38:803–807. https://doi.org/10.1007/s10295-010-0812-8

Klemm D, Kramer F, Moritz S et al (2011) Nanocelluloses: a new family of nature‐based materials. Angew Chem Int Ed 50:5438–5466. https://doi.org/10.1002/anie.201001273

Lavoine N, Desloges I, Dufresne A et al (2012) Microfibrillated cellulose – Its barrier properties and applications in cellulosic materials: a review. Carbohydr Polym 90:735–764. https://doi.org/10.1016/j.carbpol.2012.05.026

Li W, Wang S, Wang W et al (2019) Facile preparation of reactive hydrophobic cellulose nanofibril film for reducing water vapor permeability (WVP) in packaging applications. Cellulose 26:3271–3284. https://doi.org/10.1007/s10570-019-02270-x

Lyu D, Tang Y, Qian L et al (2019) Large strain cavitation induced stress whitening in propylene-butene-1 copolymer during stretching. Polymer 167:146–153. https://doi.org/10.1016/j.polymer.2019.01.081

Mandal A, Chakrabarty D (2011) Isolation of nanocellulose from waste sugarcane bagasse (SCB) and its characterization. Carbohydr Polym 86:1291–1299. https://doi.org/10.1016/j.carbpol.2011.06.030

Melro E, Antunes FE, da Silva GJ et al (2021) Chitosan films in food applications. Tuning film properties by changing acidic dissolution conditions. Polymers 13:1. https://doi.org/10.3390/polym13010001

Moon RJ, Martini A, Nairn J et al (2011) Cellulose nanomaterials review: structure, properties and nanocomposites. Chem Soc Rev 40:3941. https://doi.org/10.1039/c0cs00108b

Mäkelä T, Kainlauri M, Willberg-Keyriläinen P et al (2016) Fabrication of micropillars on nanocellulose films using a roll-to-roll nanoimprinting method. Microelectron Eng 163:1–6. https://doi.org/10.1016/j.mee.2016.05.023

Ndikumana S, Tanane O, Aichi Y et al (2025) Innovative applications of sugarcane bagasse in the global sugarcane industry. Processes 13:3796. https://doi.org/10.3390/pr13123796

Nechyporchuk O, Belgacem MN, Bras J (2016) Production of cellulose nanofibrils: a review of recent advances. Ind Crops Prod 93:2–25. https://doi.org/10.1016/j.indcrop.2016.02.016

Niskanen I, Zhang K, Karzarjeddi M et al (2022) Optical properties of cellulose nanofibre films at high temperatures. J Polym Res 29:187. https://doi.org/10.1007/s10965-022-03019-0

Nogi M, Iwamoto S, Nakagaito AN et al (2009) Optically transparent nanofiber paper. Adv Mater 21:1595–1598. https://doi.org/10.1002/adma.200803174

Nogi M, Kim C, Sugahara T et al (2013) High thermal stability of optical transparency in cellulose nanofiber paper. Appl Phys Lett 102:181911. https://doi.org/10.1063/1.4804361

Otenda BV, Kareru PG, Madivoli ES et al (2022) Cellulose nanofibrils from sugarcane bagasse as a reinforcing element in polyvinyl alcohol composite films for food packaging. J Nat Fibers 19:3585–3597. https://doi.org/10.1080/15440478.2020.1848712

Pillai C, Paul W, Sharma CP (2009) Chitin and chitosan polymers: Chemistry, solubility and fiber formation. Prog Polym Sci 34:641–678. https://doi.org/10.1016/j.progpolymsci.2009.04.001

Qing Y, Sabo R, Wu Y et al (2012) High-performance cellulose nanofibril composite films. BioResources 7:3064–3075. https://doi.org/10.15376/biores.7.3.3064-3075

Rinaudo M (2006) Chitin and chitosan: properties and applications. Prog Polym Sci 31:603–632. https://doi.org/10.1016/j.progpolymsci.2006.06.001

Rol F, Billot M, Bolloli M et al (2020) Production of 100% cellulose nanofibril objects using the molded cellulose process: a feasibility study. Ind Eng Chem Res 59:7670–7679. https://doi.org/10.1021/acs.iecr.9b06127

Saito T, Kimura S, Nishiyama Y et al (2007) Cellulose nanofibers prepared by TEMPO-mediated oxidation of native cellulose. Biomacromolecules 8:2485–2491. https://doi.org/10.1021/bm0703970

Scopel E, Pinto LO, Rezende CA (2025) Residual lignin affects production and properties of TEMPO-oxidized cellulose nanofibrils from partially delignified sugarcane bagasse. Cellulose 32:9315–9331. https://doi.org/10.1007/s10570-025-06785-4

Sehaqui H, Zhou Q, Ikkala O et al (2011) Strong and tough cellulose nanopaper with high specific surface area and porosity. Biomacromolecules 12:3638–3644. https://doi.org/10.1021/bm2008907

Sellman FA, Rostami J, Östmans R et al (2024) Influence of fibril aspect ratio, chemical functionality, and volume fraction on the mechanical properties of cellulose nanofibril materials. Cellulose 31:8007–8025. https://doi.org/10.1007/s10570-024-06084-4

Semple KE, Zhou C, Rojas OJ et al (2022) Moulded pulp fibers for disposable food packaging: a state-of-the-art review. Food Packag Shelf Life 33:100908. https://doi.org/10.1016/j.fpsl.2022.100908

Shimizu M, Saito T, Isogai A (2016) Water-resistant and high oxygen-barrier nanocellulose films with interfibrillar cross-linkages formed through multivalent metal ions. J Membr Sci 500:1–7. https://doi.org/10.1016/j.memsci.2015.11.002

Sirviö JA, Kantola AM, Komulainen S et al (2021) Aqueous modification of chitosan with itaconic acid to produce strong oxygen barrier film. Biomacromolecules 22:2119–2128. https://doi.org/10.1021/acs.biomac.1c00216

Spence KL, Venditti RA, Rojas OJ et al (2011) A comparative study of energy consumption and physical properties of microfibrillated cellulose produced by different processing methods. Cellulose 18:1097–1111. https://doi.org/10.1007/s10570-011-9533-z

Szymańska-Chargot M, Chylińska M, Pertile G et al (2019) Influence of chitosan addition on the mechanical and antibacterial properties of carrot cellulose nanofibre film. Cellulose 26:9613–9629. https://doi.org/10.1007/s10570-019-02755-9

Tao J, Fang Z, Zhang Q et al (2017) Super‐clear nanopaper from agro‐industrial waste for green electronics. Adv Electron Mater 3:1600539. https://doi.org/10.1002/aelm.201600539

Toivonen MS, Kurki-Suonio S, Schacher FH et al (2015) Water-resistant, transparent hybrid nanopaper by physical cross-linking with chitosan. Biomacromolecules 16:1062–1071. https://doi.org/10.1021/acs.biomac.5b00145

Vishtal A, Retulainen E (2012) Deep-drawing of paper and paperboard: the role of material properties. BioResources 7:4424–4450. https://doi.org/10.15376/biores.7.3.4424-4450

Wang Y, He B, Zhao L (2017) Fabrication of hydrophobic coating on filter paper from self-emulsifying carnauba wax-alcohol emulsions with nano-TiO2 particles for water/diesel separation. BioResources 12:7774–7783. https://doi.org/10.15376/biores.12.4.7774-7783

Xu X, Zhou J, Jiang L et al (2016) Highly transparent, low-haze, hybrid cellulose nanopaper as electrodes for flexible electronics. Nanoscale 8:12294–12306. https://doi.org/10.1039/c6nr02245f

Yang W, Jiao L, Liu W et al (2019) Manufacture of highly transparent and hazy cellulose nanofibril films via coating TEMPO-oxidized wood fibers. Nanomaterials 9:107. https://doi.org/10.3390/nano9010107

Zhu H, Fang Z, Preston C et al (2014) Transparent paper: fabrications, properties, and device applications. Energy Environ Sci 7:269–287. https://doi.org/10.1039/c3ee43024c